Supporting Information

Synthesis of Conjugated Polymers with Controlled Terminal Structures by Direct Arylation Polycondensation and Correlation between Terminal Structures and Emission Properties

Ziwei Hu,a Takeshi Yasuda,b Takaki Kanbara, a* Junpei Kuwabara a,c*

Scheme S1. Synthesis of the Pd(II) catalyst precursor.

Scheme S2. Polycondensation and terminal modification by the Pd(II) catalyst precursor.

Table S1. Results of polycondensation

| Entry | TPD : Br2-DOF | Yield a) | Mn (Mw/Mn) | Theoretical Mn b) |
| --- | --- | --- | --- | --- |
| 1 | 1 : 1.05 | 73% | 120 000 (2.6) | 24 600 |
| 2 | 1 : 1.33 | 77% | 16 900 (1.8) | 4 900 |

a) Yields of the CHCl3-soluble and hexane-insoluble parts. b) Calculated by the Carothers equation.

Figure S1. MALDI-TOF-MS of the polymer (Table 1, Entry 1).

Figure S2. MALDI-TOF-MS of the polymer (Table 1, Entry 2).

Figure S3. MALDI-TOF-MS of the polymer (Table 1, Entry 3).

Figure S4. 1H NMR Spectrum of the terminal modified polymer (600 MHz, CDCl3, r.t.).

Figure S5. MALDI-TOF-MS tracking the terminal modification process using Pd(PCy3)2.

Figure S6. 1H NMR spectrum of the Pd(II) catalyst precursor. (400 MHz, CDCl3).

Figure S7. 13C{1H} NMR spectrum of the Pd(II) catalyst precursor (100 MHz, CDCl3).

Figure S8. 31P NMR spectrum of the Pd(II) catalyst precursor (162 MHz, CDCl3).

Figure S9. 1H NMR spectrum of P-Th (600 MHz, C2D2Cl4, 373 K).

Figure S10. 1H NMR spectrum of P-TPD (600 MHz, C2D2Cl4, 373 K).

Figure S11. 1H NMR spectrum of P-Br (600 MHz, C2D2Cl4, 373 K).

Figure S12. UV-Vis absorption spectra (a) in the solution (CHCl3, 5 μM) and (b) thin-film states.

Figure S13. Voltage (V) – Luminance (L) characteristics of the OLEDs.

Figure S14. Normalized EL spectrum of the OLED with P-TPD and PL spectrum in thin-film state.