## Slide 1
Harvesting radiative cooling and solar heating
with transparent thermoelectric device
Designs for harvesting radiative cooling and solar heating
Satoshi Ishii,1,2 Cédric Bourgès,1,3 Nicholaus K. Tanjaya,1,2 Takao Mori1,2
1 Research Center for Materials Nanoarchitectonics (MANA), National Institute for Materials Science (NIMS),, Japan
2 Subprogram in Materials Science and Engineering, Graduate School of Science and Technology, University of Tsukuba, Japan
3 International Center for Young Scientists, National Institute for Materials Science (NIMS), Japan
sishii@nims.go.jp
Optical properties and thermoelectric performances
Satoshi Ishii, Cédric Bourgès, Nicholaus K. Tanjaya, Takao Mori, Mater. Today 75, 20-26 (2024)
Abstract
A thermoelectric device which can simultaneously harvest radiative cooling and solar heating is presented. By sandwiching the transparent thermoelectric module by a transparent plate at the top and a black plate at the bottom, the device is capable of harvesting radiative cooling and solar heat with the co-planar geometry in day and harvesting radiative cooling in night confirmed by outdoor and indoor measurements. Our device can be an efficient method to judiciously harvesting solar heating and radiative cooling simultaneously, paving the way for efficient energy harvesters which can be used as stand-alone power supplies for off-gird sensor modules.
, , ,
, , ,
Thermoelectric generation (TEG) by radiative cooling to the sky
⇔ Sunlight reflection by daytime radiative cooler
Harvesting radiative cooling & solar heating in day for TEG
⇔ Solar absorbers and radiative coolers are non-coplanar
Solar absorbers and radiative coolers are coplanar
⇒ Improving TEG per unit area
Transparent thermoelectric materials allow coplanar design
⇒ IGZO as n-type, CuI as p-type TE thin films
IGZO and CuI fabricated on each side of the glass substrate are transparent
Blackbody paint: absorptive in VIS-NIR & MIR
PET sheet: transparent in VIS-NIR, absorptive in MIR
Simultaneously harvesting radiative cooling and solar heating for TEG with the coplanar structure confirmed by indoor and outdoor measurements
1. S. Ishii, et al, Sci. Technol. Adv. Mater., 2021, 22, 441-448; 2. K. Gao, et al, Solar RRL, 2022, 6, 2100975; 3. S. Zhang, et al, Adv. Mater. Technol., 2022, 7, 2200478; 4. W. B. Han, et al, Sci. Adv., 2023, 9, eadf5883.
Past works
This work
IGZO/glass/CuI