Supporting Information

Ammonia Cracking Catalyzed by Ni Nanoparticles Confined in the Framework of CeO2 Support

Hiroshi Mizoguchi,1,Ⅱ,* Yuta Osawa,1,Ⅱ Masato Sasase,2 Naoki Ohashi,3 Masaaki Kitano,2 and

Hideo Hosono1, 2, *

1Research Center for Materials Nanoarchitectonics (MANA),

National Institute for Materials Science (NIMS)

  - Namiki, Tsukuba, Ibaraki 305-0044, Japan

2MDX Research Center for Element Strategy, International Research Frontiers Initiative,

Tokyo Institute of Technology,

4259 Nagatsuta, Midori-ku, Yokohama 226-8503, Japan

3Research Center for Electronic and Optical Materials,

National Institute for Materials Science (NIMS)

  - Namiki, Tsukuba, Ibaraki 305-0044, Japan

ⅡThese authors contributed equally to this work

*Corresponding author footnote: MIZOGUCHI.Hiroshi@nims.go.jp, hosono@mces.titech.ac.jp

Table S1. Catalytic performance of Ni-based catalysts for NH3 cracking under 1 atm.

| Ni wt% | support | promoter | WHSV (mL g-1h-1) | GHSV (h-1) | T (℃) | conv (%) | ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 63 | CeO2 |  | 10000 |  | 400 | 22 | This work |
| 72 | YO1.5 |  | 10000 |  | 400 | 26 | This work |
| 58 | Al2O3 |  | 30000 |  | 450 | 15 | 1 |
| 10 | Al2O3 |  | 240000 | 80000 | 500 | 93 | 2 |
| 10 | Al2O3 |  | 9000 |  | 400 | 32 | 3 |
| 58 | Al2O3 | Ce | 30000 |  | 450 | 28 | 1 |
| 5 | C |  |  | 13000 | 400 | 19 | 4 |
| 10 | GNP |  | 15000 | 12000 | 375 | 17 | 5 |
| 58 | Al2O3 | La | 30000 |  | 450 | 26 | 6 |
| 20 | MgO | La | 22000 |  | 400 | 28 | 7 |
| 7 | MCM-41 |  | 36000 |  | 500 | 58 | 8 |
| 10 | CaNH |  | 15000 |  | 400 | 19 | 9 |

Fig. S1. (a) Time course of NH3 cracking over RNi5 (R = Ce or Y). (b) WHSV dependance of the conversion in NH3 cracking over CeNi5. As the WHSV increased, the activity decreased because of the shortening of the contact time between the catalyst and the NH3 molecule.

Fig. S2. Insertion and deinsertion of oxygen in CeNi5 to enhance IM thermal decomposition at atomic scale.

Fig. S3. Halder–Wagner plot of Ni phase in CeNi5 catalyst to determine CS. β is spread of integral peak width.

Fig. S4. TDS spectra at a specific mass-to-charge (m/z) of 2 (H2), 17 (NH3), or 28 (N2)

for RNi5 catalysts after NH3 reaction (R = Ce (a) or Y (b)).

Fig. S5. Temperature dependence of the conversion in NH3 cracking over various Ni-based catalysts at a WHSV of 10000 mLNH3 gcat-1 h-1. The effect of BM is shown.

REFERENCES

1.	Zheng, W.;  Zhang, J.;  Ge, Q.;  Xu, H.; Li, W., Effects of CeO2 Addition on Ni/Al2O3 Catalysts for the Reaction of Ammonia Decomposition to Hydrogen. Appl. Catal. B: Environ. 2008, 80 (1-2), 98-105.

2.	Simonsen, S. B.;  Chakraborty, D.;  Chorkendorff, I.; Dahl, S., Alloyed Ni-Fe Nanoparticles as Catalysts for NH3 Decomposition. Appl. Catal. A: General 2012, 447-448, 22-31.

3.	Han, X.;  Chu, W.;  Ni, P.;  Luo, S.; Zhang, T., Promoting Effects of Iridium on Nickel Based Catalyst in Ammonia Decomposition. J. Fuel Chem. Tech. 2007, 35, 691-695.

4.	Bramwell, P. L.;  Lentink, S.;  Ngene, P.; de Jongh, P. E., Effect of Pore Confinement of LiNH2 on Ammonia Decomposition Catalysis and the Storage of Hydrogen and Ammonia. J. Phys. Chem. C 2016, 120 (48), 27212-27220.

5.	Chang, F.;  Wu, H.;  Pluijm, R. V.;  Guo, J.;  Ngene, P.; de Jongh, P. E., Effect of Pore Confinement of NaNH2 and KNH2 on Hydrogen Generation from Ammonia. J. Phys. Chem. C Nanomater Interfaces 2019, 123 (35), 21487-21496.

6.	Zhang, J.;  Xu, H.;  Jin, X.;  Ge, Q.; Li, W., Characterizations and Activities of the Nano-sized Ni/Al2O3 and Ni/La–Al2O3 Catalysts for NH3 Decomposition. Appl. Catal. A: General 2005, 290 (1-2), 87-96.

7.	Hu, X.;  Wang, W.;  Jin, Z.;  Wang, X.;  Si, R.; Jia, C., Transition Metal Nanoparticles Supported La-Promoted MgO as Catalysts for Hydrogen Production via Catalytic Decomposition of Ammonia. J. Energy Chem. 2019, 38, 41-49.

8.	Duan, X.;  Qian, G.;  Liu, Y.;  Ji, J.;  Zhou, X.;  Chen, D.; Yuan, W., Structure Sensitivity of Ammonia Decomposition over Ni Catalysts: A Computational and Experimental Study. Fuel Process. Tech. 2013, 108, 112-117.

9.	Ogasawara, K.;  Nakao, T.;  Kishida, K.;  Ye, T.;  Lu, Y.;  Abe, H.;  Niwa, Y.;  Sasase, M.;  Kitano, M.; Hosono, H., Ammonia Decomposition over CaNH-Supported Ni Catalysts via an NH2--Vacancy-Mediated Mars-van Krevelen Mechanism. ACS Catal. 2021, 11, 11005-11015.