Supporting Information

# Facile Synthesis of FeSe2/rGO with High Reaction Kinetic for Simultaneously Ultrafast and Durable Sodium Storage

Guangxu Xu1,2, Wenfeng Cui1,2, Hang Yin2,3, Naoki Fukata1,2,*, Jie Tang2,3,*

1Research Center for Materials Nanoarchitectonics (MANA), National Institute for Materials Science, 1-1 Namiki, Tsukuba, Ibaraki 305-0044, Japan

2University of Tsukuba, 1-1-1 Tennodai, Tsukuba, Ibaraki 305-0006, Japan

3National Institute for Materials Science, 1-2-1 Sengen, Tsukuba, Ibaraki 305-0047, Japan

Corresponding authors

Email: FUKATA. Naoki@nims.go.jp (Naoki Fukata), TANG. Jie@nims.go.jp (Jie Tang)

Figure S1. Full XPS survey of FeSe2/rGO.

Figure S2. (a) N2 adsorption and desorption isotherms, and (b) pore size distribution of FeSe2/rGO and FeSe2.

Figure S3. (a) EIS curves of FeSe2 in ether-based electrolyte at different temperatures, and (b) EIS curves of FeSe2/rGO in ester-based electrolyte at different temperatures.

Figure S4. (a) explanation of GITT, (b) the calculated Na+ diffusion coefficient of FeSe2/rGO and FeSe2 with different electrolytes during charge process.

DNa+=4πτnmVmS2∆E1∆E22                         (S1)

τ represents the relaxation time(s), nm(mol) and Vm(cm3/mol) stand for the molar number and molar volume of active materials, respectively, and S is the electrode area. ∆E1 and ∆E2 are shown in Figure S4a, representing the voltage change after the relax time and after the pulse time.

Figure S5. (a) in-situ EIS curves and (e) corresponding DRT distribution maps of FeSe2/rGO in ester-based electrolyte

Figure S6. (a) in-situ EIS curves and (e) corresponding DRT distribution maps of FeSe2/rGO in ether-based electrolyte in 100th cycle.

Figure S7. Detail capacitive contribution of FeSe2/rGO at 1.0 mV s-1.

Figure S8. (a-b) SEM images of AC electrode.

Figure S9. (a) CV curves at 0.2 mV s-1 in the first three cycles, (b) Rate performance, and (c) Cycle performance at 2 A g-1 of AC.

Figure S10. Rate performance of FeSe2/rGO//AC SICs.

Table S2 Cycling performance comparison of this work with reported FeSe2-based materials

| Materials | Current density (A g-1) | Cycle number |  | Specific Capacity (mAh g-1) |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| FeSe2/rGO | 5 |  | 4500 |  | 498 | this work |
|  | 10 |  | 9000 |  | 491 |  |
| FeSe2@NC | 5 | 1000 |  | 447.3 |  | [1] |
| FeSe2-CoSe2@NC/CNT | 1 | 500 |  | 300.1 |  | [2] |
| Co-FeSe2@C | 2 | 6800 |  | 336.3 |  | [3] |
| HT-FeSe2/Se/C | 1 | 125 |  | 325.3 |  | [4] |
| (Co,Fe)Se-NGC@PDA-20 | 1 | 200 |  | 306 |  | [5] |
| FeSe2@C2 | 1 | 500 |  | 204.2 |  | [6] |
| CoSe2/FeSe2@NC | 5 | 5000 |  | 366.6 |  | [7] |

References

[1] S. Zhou, R. Jiang, S. Wang, L. Yu, X. Shi, L. Shao, Z. Sun, L. Hang, FeSe2 micro-nanorods confined in N-doped carbon as an advanced anode for fast sodium ion storage, J. Mater. Chem. A 12 (2024) 11028-11037.

[2] J.T. Lei, W.X. Wen, P.P. Chen, Y.J. Ren, Z.A. Li, J.Z. Chen, D.L. Zhao, Carbon Nanotube Intertwined Nano-Nested Heterojunction Cubes with Double Shell Layers FeSe2-CoSe2@NC for Efficient Lithium/Sodium Ion Storage Anode, Small 21 (2025) 2500326.

[3] Y. Dai, X. Li, X. Sang, Y. He, S. Gu, J. Li, G. Zhou, X. Wang, B. Sun, Y. He, Cobalt-doped iron-based selenide for sodium-ion battery anode: Insight into the doping and sodium storage mechanism, Chem. Eng. J. 511 (2025) 161949.

[4] H. Fan, Z. Yang, Z. Cheng, F. Bahmani, J. Zhang, X.L. Wu, Enhanced redox kinetics in hierarchical tubular FeSe2 by incorporating Se quantum dots towards high-performance sodium-ion batteries, J. Colloid Interface Sci 667 (2024) 303-311.

[5] N. Kitchamsetti, J. Sang Cho, C. Shilpa Chakra, Prussian blue analogue derived porous hollow nanocages comprising polydopamine-derived N-doped C coated CoSe2/FeSe2 nanoparticles composited with N-doped graphitic C as an anode for high-rate Na-ion batteries, Chem. Eng. J. 495 (2024) 153353.

[6] J. Luo, S. Bo, S. Park, B.-K. Park, O.L. Li, Plasma-engineered FeSe2-encapsulated carbon composites with enhanced kinetics for high-performance lithium and sodium ion batteries, Carbon Lett. 34 (2024) 2421-2433.

[7] Z. Lin, Z. Wu, M. Yu, H. Jia, K. Zhou, X. Huang, S. Ying, Fabrication of CoSe2/FeSe2 heterostructures with a stable solid-electrode interphase film and low surface activation energy for Na-ion batteries, J. Mater. Chem. A 13 (2025) 5830-5838.