Supplementary Material for

Modification of Platinum Surfaces with Cerium Species for Promoting Oxidative Desorption of Adsorbed Sulfur

Tetsuro Morooka, Tamao Shishido, Takuya Nakanishi, Takuya Masuda

Research Center for Energy and Environmental Materials (GREEN), National Institute for Materials Science (NIMS), Tsukuba, Ibaraki 305-0044, Japan.

Figure S1. CVs of the Ce-free (black) and Ce-modified (red) Pt(111) surfaces measured in a 0.1 M HClO4 aqueous solution at a scan rate of 50 mV/s.

Figure S2. CVs of polycrystalline Pt electrode after being immersed in Ce(NO3)3 aqueous solution with (a) Ar/H2 gas bubbling and (b) holding the potential at −0.2 V vs. Ag/AgCl and (c) without Ar/H2 gas bubbling, and after (d) drop-casting Ce(NO3)3 aqueous solution (red), together with those of pristine polycrystalline Pt surface (black) in 0.1 M HClO4 aqueous solution saturated with Ar/H2 gas with a scan rate of 50 mV s-1.