Supporting Information

Room temperature large magnetodielectric and magnetoimpedance in (NiMnFeAlZn)3O4 high entropy oxide

Alok Kumar Sahu, Sananda Das, Sanjay Tamang, Y. K. Takahashi, Perumal Alagarsamy

Table S1: Binding energy (in eV) of different elements extracted from the XPS spectra for (NiMnFeAlZn)3O4 HEO.

Figure S1: Modified Arrott Plot M1/β vs.  μ0HM1/γ for (NiMnFeAlZn)3O4 HEO with the reliable critical exponents. The line passing through the origin is marked as TC.

Figure S2: (a) MSP(T) and χ0-1(T) curves versus temperature for (NiMnFeAlZn)3O4 HEO. The solid lines are the best fits according to eqns.(2) and (3). (b) The Kouvel-Fisher plot for MSP(T) and χ0-1(T). The solid lines are the best fits according to eqn.(5) and (6). (c) Log-Log scale isothermal M(0H) plot. The solid line is the best fit to eqn.(4).

Table S2: Comparison of the critical exponent values of (NiMnFeAlZn)3O4 HEO with those of the standard models and with some other spinel materials.

Table S3: The comparison of material type and transition temperature of the currently investigated (NiMnFeAlZn)3O4 HEO with the other similar materials.

Figure S3: χ-1(T) vs. T for (NiMnFeAlZn)3O4 HEO. The solid line is the fit to the eqn. (8).

Table S4: The ratio of valence states of 2+ and 3+, cation concentration, and the effective magnetic moment (μeff.) of individual elements for (NiMnFeAlZn)3O4 HEO.

Figure S4: M(H) loop at 300 K for (NiMnFeAlZn)3O4 HEO. For comparison, magnetization data extracted from M(T) curves under different applied magnetic fields at 300 K are also shown. The inset provides an expanded view near the origin, highlighting the hysteresis loop.

Figure S5: Initial magnetization curve at 5 K fitted to the law of approach to saturation model for (NiMnFeAlZn)3O4 HEO.

Figure S6: Temperature-dependent tan  (in log scale) at different frequencies for (NiMnFeAlZn)3O4 HEO.

Table S5: The comparison of the material’s magnetodielectric (MD) (%) and magnetoimpedance (MZ) (%) of the currently investigated (NiMnFeAlZn)3O4 HEO with the other similar materials.

Table S1: Binding energy (in eV) of different elements extracted from the XPS spectra for (NiMnFeAlZn)3O4 HEO.

| Element | Electronic state | Spectra | Binding Energy (eV) | Spin-orbit splitting (eV) |
| --- | --- | --- | --- | --- |
| Mn 2p | 2+ | 2p1/2 | 653.00 | 11.54 |
|  |  | 2p3/2 | 641.46 |  |
|  | 3+ | 2p1/2 | 653.90 |  |
|  |  | 2p3/2 | 642.45 |  |
| Ni 2p | 2+ | 2p1/2 | 872.30 | 17.79 |
|  |  | 2p3/2 | 854.51 |  |
|  | 3+ | 2p1/2 | 875.17 |  |
|  |  | 2p3/2 | 855.56 |  |
| Fe 2p | 2+ | 2p1/2 | 723.41 | 13.07 |
|  |  | 2p3/2 | 710.34 |  |
|  | 3+ | 2p1/2 | 725.43 |  |
|  |  | 2p3/2 | 712.81 |  |
| Zn 2p | 2+ | 2p1/2 | 1043.66 | -- |
|  |  | 2p3/2 | 1020.59 |  |
|  | 3+ | 2p1/2 | -- |  |
|  |  | 2p3/2 | -- |  |
| Al 2p | 2+ | 2p1/2 | -- | -- |
|  |  | 2p3/2 | -- |  |
|  | 3+ | 2p1/2 | -- |  |
|  |  | 2p3/2 | 73.21 |  |
| O 1s | 2- | 1s | 529.63 | -- |
|  | 1- | 1s | 531.69 |  |
|  | Others (-OH) | -- | 532.65 |  |

Figure S1: Modified Arrott Plot M1/β vs.  μ0HM1/γ for (NiMnFeAlZn)3O4 HEO with the reliable critical exponents. The line passing through the origin is marked as TC.

Modified Arrott Plot method:

The isothermal magnetization data collected near the transition temperature were analysed using the Modified Arrott Plot (MAP) method to extract the critical exponents. This approach employs the following relation

| μ0HM1γ=aη+bM1β ;η=T-TCTC | (1) |
| --- | --- |

where a and b are constants, η is the reduced temperature, and  and  are critical exponents. To determine reliable values of the critical exponents for the investigated samples,  and  values were systematically tuned such that the plot of M1β vs. μ0HM1γ exhibit linear behavior in the high field region. Additionally, the isotherm corresponding to T=TC was constrained to pass through the origin, ensuring consistency with the scaling hypothesis. This criterion was satisfied when the critical exponent values were set to  = 0.39 and  = 1.026.

Figure S2: (a) MSP(T) and χ0-1(T) curves versus temperature for (NiMnFeAlZn)3O4 HEO. The solid lines are the best fits according to eqns.(2) and (3). (b) The Kouvel-Fisher plot for MSP(T) and χ0-1(T). The solid lines are the best fits according to eqn.(5) and (6). (c) Log-Log scale isothermal M(0H) plot. The solid line is the best fit to eqn.(4).

To clarify the nature of the ferrimagnetic to paramagnetic phase transition in the (NiMnFeAlZn)3O4 HEO, a detailed study of the critical exponents (,,) around the transition temperature is conducted using the power law [1] as described in eqns.(2) to (4)

| MSPT=M0-ηβ ; η=T-TCTC<0 | (2) |
| --- | --- |
| χ0-1T=χ0ηγ ; η=T-TCTC>0 | (3) |
| M=M0μ0H1/δ ;η=0; T=TC | (4) |

and Kouvel-Fisher method [1] defined in the eqns.(5) to (6).

| MSPTdMSPTdT-1=T-TCβ | (5) |
| --- | --- |
| χ0-1Tdχ0-1TdT-1=T-TCγ | (6) |

While the obtained critical exponent  is close to the mean-field model [1], the other two critical exponents  and  do not match with any conventional model, but exhibit close agreement with Widom’s scaling relation [2] given by

| δ=1+γβ=3.597 | (7) |
| --- | --- |

The obtained critical exponents, along with those for the standard models and other similar spinel oxide materials, are presented in Table S2 for comparison.

Table S2: Comparison of the critical exponent values of (NiMnFeAlZn)3O4 HEO with those of the standard models and with some other spinel materials.

| Material | Technique | TC (K) |  |  |  | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Mean-field model |  |  | 1.0 | 0.5 | 3.0 | [1] |
| 3D-Heisenberg model |  |  | 1.336 | 0.365 | 4.80 | [1] |
| 3D-Ising model |  |  | 1.24 | 0.325 | 4.82 | [1] |
| Tricritical mean-field model |  |  | 1.0 | 0.25 | 5.0 | [3] |
| (NiMnFeAlZn)3O4 | MAP | 217.5 |  | 0.395 |  | Present work |
|  |  | 217.9 | 1.026 |  |  | Present work |
|  | KF | 217.7 |  | 0.401 |  | Present work |
|  |  | 217.4 | 1.015 |  |  | Present work |
|  | LL |  |  |  | 3.626 | Present work |
|  | WSR |  |  |  | 3.597 | Present work |
| MnCr2O4 |  | 42.88 | 1.0256 | 0.3932 | 3.55 | [4] |
| Ni0.5Mn0.5Cr2O4 |  | 38 | 1.00 | 0.99 | 2.01 | [5] |
| Ni0.5Fe0.5Cr2O4 |  | 90.19 | 0.768 | 0.496 | 2.779 | [6] |
| La0.4Pr0.3Ba0.3MnO3 |  | 244 | 1.092 | 0.694 | 2.672 | [7] |
| MnV2O4 |  | 60 | 0.909 | 0.349 | 2.913 | [8] |
| Cu1.5Mn1.5O4 |  | 78.65 | 1.21 | 0.313 | 4.54 | [9] |
| TbCo1.9Fe0.1 |  |  |  |  |  | [10] |

MAP – Modified Arrott Plot; KF – Kouvel-Fisher method; LL – Log-Log scale plot at critical isotherm; WSR – Widom’s Scaling relations

Table S3: The comparison of material type and transition temperature of the currently investigated (NiMnFeAlZn)3O4 HEO with the other similar materials.

| Sl. | Material | Type* | Transition Temperature | Ref. |
| --- | --- | --- | --- | --- |
| 1 | (CoCuMgNiZn)O | AFM | TN = 106 K, 113K, 700 K | [11], [12] |
| 2 | (CoCrFeMnNi)3O4 | FiM | 420 K | [13] |
| 3 | (Fe6Ti1·2Co1·2In1.2Ga1.2Cr1.2)O19 | PM | 300 K | [14] |
| 4 | La(CoCrFeMnNi)O3 | AFM | TN = 185 K | [15] |
| 5 | (CrFeMnCoNi)3O4 | AFM | TN = (110-180) K | [15], [16] |
|  | (CrFeMnZnNi)3O4 |  |  |  |
|  | (CrFeMnCoZn)3O4 |  |  |  |
|  | A(CrFeMnCoNi)3O4 (A=Y, Gd, A, Sm, Nd, La) |  |  |  |
| 6 | (AlCoCrFeMnNi)3O4 | FM | TC = 248 K | [17] |
| 7 | (NiMnFeAlZn)3O4 | FiM | TC = 217.5 K | Present work |
| *AFM - Antiferromagnet, FiM - Ferrimagnet, FM - Ferromagnet, PM - Paramagnet |  |  |  |  |

Figure S3: χ-1(T) vs. T for (NiMnFeAlZn)3O4 HEO. The solid line is the fit to the eqn. (8).

To gain deeper insight into the ferrimagnetic behavior of the system, the temperature-dependent inverse susceptibility data, χ-1(T) were analyzed using the modified Curie-Weiss law based on Néel’s molecular field theory, as defined in eqn.(8) [6,18].

| χ-1(T)=T-θ'C-ξT-θ" | (8) |
| --- | --- |

Where, θ, C, ξ and θs are the asymptotic Curie temperature, Curie constant, curvature of inverse susceptibility graph, and characteristic temperature (!217.5 K estimated from modified Arrott plot method). The fitting procedure resulted in the value of the Curie constant, C, as 4.64 emu K mol-1 Oe-1. The experimental effective paramagnetic moment μeff(exp.) was calculated from the Curie constant, C, using eqn.(9).

| μeff(exp.)=3kBCNA | (9) |
| --- | --- |

where kB and NA are the Boltzmann constant (=1.38×10-16 ergs.K-1) and Avogadro’s number (=6.023×1023 per mole), respectively. The resulting value, μeff(exp.)=6.09 μB/f.u. shows good agreement with the theoretically estimated value μeff(th.)=6.23 μB/f.u., calculated by considering the high-spin Mn, Ni3+, and Fe, along with low-spin Ni2+, as expressed in eqn.(10).

| μeff(Th.)=0.36μMn2+2+0.40μNi2+2+0.33μFe2+2+0.24μMn3+2+0.20μNi3+2+0.27μFe3+2 | (10) |
| --- | --- |

This close correspondence between experimental and theoretical values confirms that Mn, Ni³⁺, and Fe ions are in the high-spin state, while Ni²⁺ adopts a low-spin configuration.

Table S4: The ratio of valence states of 2+ and 3+, cation concentration, and the effective magnetic moment (μeff.) of individual elements for (NiMnFeAlZn)3O4 HEO.

| Cation | Valence states (%) |  | Cation concentration in Spinel* |  | μeff. |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 2+ | 3+ | 2+ | 3+ | 2+ | 3+ |
| Mn | 60.46 | 39.54 | 0.36 | 0.24 | 5.92 (HS) | 4.90 (HS) |
| Ni | 66.57 | 33.43 | 0.40 | 0.20 | 0 (LS) | 3.87 (HS) |
| Fe | 55.23 | 44.77 | 0.33 | 0.27 | 4.92 (HS) | 5.92 (HS) |

HS = High Spin, LS = Low Spin

*Zn2+ and Al3+ have each a concentration of 0.6 in (NiMnFeAlZn)3O4 HEO. However, due to its nonmagnetic nature, it is not included in the table above.

Figure S4: M(H) loop at 300 K for (NiMnFeAlZn)3O4 HEO. For comparison, magnetization data extracted from M(T) curves under different applied magnetic fields at 300 K are also shown. The inset provides an expanded view near the origin, highlighting the hysteresis loop.

Figure S5: Initial magnetization curve at 5 K fitted to the law of approach to saturation model for (NiMnFeAlZn)3O4 HEO.

To extract the saturation magnetization, the initial magnetization curve obtained at 5 K is fitted with the law of approach to saturation model [19], as expressed in eqn.(11).

| M=MS1-8keff2105μ02MS2H2+χhfμ0H | (11) |
| --- | --- |

where MS is the saturation magnetization, keff is the effective magnetic anisotropy, hf is the high-field susceptibility.

Figure S6: Temperature-dependent tan  (in log scale) at different frequencies for (NiMnFeAlZn)3O4 HEO.

Table S5: The comparison of the material’s magnetodielectric (MD) (%) and magnetoimpedance (MZ) (%) of the currently investigated (NiMnFeAlZn)3O4 HEO with the other similar materials.

| Sl. | Material | MD (%) | MZ (%) | Ref. |
| --- | --- | --- | --- | --- |
| 1 | La0.4Dy0.1Ca0.5MnO3 | -27% (0.6 T, all f, RT); -40% (1.2 T, all f, RT) | -8% (0.6 T, all f, RT) -10% (1.2 T, low f, RT) -12% (1.2 T, high f, RT) | [20] |
| 2 | Y2.7La0.3Fe5O12 | -5% (0.9 T, 106 Hz, RT) | ---- | [21] |
| 3 | BaCo2Si2O7 | 0.2% (8 T, 100 KHz, 5.5K) | ---- | [22] |
| 4 | Bi0.85La0.15Fe0.9Co0.1O3 | 1.8% (0.8 T, 10 kHz, RT) | ---- | [23] |
| 5 | Bi4.25La0.75Fe0.5Co0.5Ti3O15 | 8.1% (1 T, 1 kHz, RT) | ---- | [24] |
| 6 | La1.2Bi0.8Mn1.2Co0.8O6.02 | 0.25% (5 T, 500 kHz, 80 K) | ---- | [25] |
| 7 | Bi0.88La0.05Lu0.7FeO3 | 2.3% (0.8 T, 1 kHz, RT) | ---- | [26] |
| 8 | [Dy(L)2(C2H5OH)Cl3]·C2H5OH | 0.75% (8 T, 10 kHz, 2 K) | ---- | [27] |
| 9 | Cu2O-CuO | -14% (9 T, 20 kHz, 320 K) | ---- | [28] |
| 10 | NdFeO3 | -19% (2 T, 1 kHz, RT) | ---- | [29] |
| 11 | (NiMnFeZAl)3O4 | ~10.3% (2.2 T, 14kHz, RT) | -13% (2.2T, 600Hz, RT) | Present work |
| *f - frequency, RT - Room Temperature. |  |  |  |  |

References

[1].	S.N. Kaul, “Static critical phenomena in ferromagnets with quenched disorder,” J. Magn. Magn. Mater., 53, 5 (1985). https://doi.org/10.1016/0304-8853(85)90128-3

[2].	B. Widom, “Equation of State in the Neighborhood of the Critical Point,” J. Chem. Phys., 43, 3898 (1965). https://doi.org/10.1063/1.1696618

[3].	H. Huang, Statistical Mechanics, 2nd Edition, Wiley, New York, (1987).

[4].	K. Dey, A. Indra, S. Majumdar, S. Giri, “Critical behavior and reversible magnetocaloric effect in multiferroic MnCr2O4,” J. Magn. Magn. Mater., 435, 15 (2017). http://dx.doi.org/10.1016/j.jmmm.2017.03.068

[5].	R. Borah, S. Ravi, “Magnetocaloric effect and critical behavior of Ni1−xMnxCr2O4 (x = 0, 0.10, and 0.50) compounds,” J Appl. Phys., 128, 233901 (2020). https://doi.org/10.1063/5.0021894

[6].	B. Alzahrani, K. Amira, S. Hcini, M.M. Almoneef, M.H. Dhaou, A. Mallah, M.L. Bouazizi, J. Khelifi, “Synthesis and study of microstructural analysis, magneto-optical properties, magnetocaloric and critical behaviors for the Ni0.5Fe0.5Cr2O4 spinel chromite,” J. Mater. Sci.: Mater. Electron., 33, 11365 (2022). https://doi.org/10.1007/s10854-022-08109-9

[7].	D. Mazumdar, K. Das, I. Das, “Study of magnetocaloric effect and critical exponents in polycrystalline La0.4Pr0.3Ba0.3MnO3 compound,” J Appl. Phys. 127, 093902 (2020). https://doi.org/10.1063/1.5142337

[8].	L. Zhang, H. Han, Z. Qu, J. Fan, L. Ling, C. Zhang, L. Pi, Y. Zhang, “Critical behavior of spinel MnV2O4 investigated by dc-magnetization,” J Appl. Phys., 115, 233910 (2014). https://doi.org/10.1063/1.4884339

[9].	A. Hadded, J. Massoudi, S. Gharbia, E. Dhahri, A. Tozrib, M.R. Berber, “Study of physical properties of a ferrimagnetic spinel Cu1.5Mn1.5O4: spin dynamics, magnetocaloric effect and critical behavior,” RSC Advances 11 25664 (2021). https://doi.org/10.1039/D1RA03732C

[10].	M. Halder, S.M. Yusuf, M. D. Mukadam, K. Shashikala, “Magnetocaloric effect and critical behavior near the paramagnetic to ferrimagnetic phase transition temperature in TbCo2−𝑥Fe𝑥,” Phys. Rev. B, 81, 174402 (2010).

https://doi.org/10.1103/PhysRevB.81.174402

[11]	A. Mao, F. Quan, H.Z. Xiang, Z.G. Zhang, K. Kuramoto, H. Yu, and S. Ran, “Solution combustion synthesis and magnetic property of rock-salt (Co0.2Cu0.2Mg0.2Ni0.2Zn0.2)O high-entropy oxide nanocrystalline powder,” J. Magn. Magn. Mater., 484, 245 (2019). https://doi.org/10.1016/j.jmmm.2019.04.023

[12]	N.J. Usharani, A. Bhandarkar, S. Subramanian, and S.S. Bhattacharya, “Antiferro-magnetism in a nanocrystalline high entropy oxide (CoCuMgNiZn)O: Magnetic constituents and surface anisotropy leading to lattice distortion,” Acta Mater., 200, 526 (2020). https://doi.org/10.48550/arXiv.2004.11684

[13].	A. Mao, F. Quan, H.Z. Xiang, Z.G. Zhang, K. Kuramoto, and A.L. Xiaa, “Facile synthesis and ferrimagnetic property of spinel (CoCrFeMnNi)3O4 high-entropy oxide nanocrystalline powder,” J. Mol. Struct., 1194, 11 (2019).

https://doi.org/10.1016/j.molstruc.2019.05.073

[14].	D.A. Vinnika, E.A. Trofimova, V.E. Zhivulina, O.V. Zaitsevaa, S.A. Gudkovaa, A.Yu. Starikova, D.A. Zherebtsova, A.A. Kirsanovaa, M. Häßnerd, and R. Niewa, “High-entropy oxide phases with magnetoplumbite structure,” Ceram. Int., 45, 12942 (2019). https://doi.org/10.1016/j.ceramint.2019.03.221

[15].	R. Witte, A. Sarkar, R. Kruk, B. Eggert, R.A. Brand, H. Wende, and H. Hahn, “High-entropy oxides: An emerging prospect for magnetic rare-earth transition metal perovskites,” Phys. Rev. Mater., 3, 1 (2019).

https://doi.org/10.1103/PhysRevMaterials.3.034406

[16].	Y. Sharma, Q. Zheng, A.R. Mazza, E. Skoropata, T. Heitmann, Z. Gai, B. Musico, P.F. Miceli, B.C. Sales, V. Keppens, M. Brahlek, and T.Z. Ward, “Magnetic anisotropy in single-crystal high-entropy perovskite oxide La(Cr0.2Mn0.2Fe0.2Co0.2Ni0.2)O3 films,” Phys. Rev. Mater., 4, 14404 (2020).

https://doi.org/10.1103/PhysRevMaterials.4.014404

[17].	A. Mao, H.X. X. Experiment, H.Z.X. Experiment, Z.G. Zhang, H. Zhang, S. Ran, “A novel six-component spinel-structure high-entropy oxide with ferrimagnetic property,” J. Magn. Magn. Mater., 503, 166594 (2020).

https://doi.org/10.1016/j.jmmm.2020.166594

[18].	K.P. Patra, S. Ravi, “Effect of chromium in magnetic and dielectric properties of inverse spinel FeMn2O4,” Appl. Phys. A, 128, 289 (2022).

https://doi.org/10.1007/s00339-022-05401-7

[19].	H. Kronmüller, “General Micromagnetic Theory and Applications. In Materials Science and Technology, eds R.W. Cahn, P. Haasen, E.J. Kramer, (2025). https://doi.org/10.1002/9783527603978.mst0460

[20]	A. Krichene, W. Boujelben, K. N. Rathod, K. Gadani, C. Chen, A. Kandasami, N.A. Shah, P.S. Solanki, “Electronic structure and room temperature colossal magnetodielectric effect in La0.4Dy0.1Ca0.5MnO3 manganite,” J. Alloys Compd., 999, 175022 (2024). https://doi.org/10.1016/j.jallcom.2024.175022

[21]	H. Wu, F. Huang, T. Xu, R. Ti, X. Lu, Y. Kan, X. Lv, W. Zhu, J. Zhu, “Magnetic and magnetodielectric properties of Y3-xLaxFe5O12 ceramics,” J Appl. Phys., 117, 5–10 (2015). https://doi.org/10.1063/1.4917218

[22]	M. Akaki, F. Nakamura, D. Akahoshi, H. Kuwahara, “Magnetodielectric effects in low-dimensional cobalt oxides,” Physica B Condens. Matter, 403, 1505-1507 (2008). https://doi.org/10.1016/j.physb.2007.10.178

[23]	S. Shankar, M. Kumar, S. Kumar, O. P. Thakur, A. K. Ghosh, “Enhanced multiferroic properties and magneto-dielectric effect analysis of La/Co modified BiFeO3,” J. Alloys Compd., 694, 715–720 (2017).

https://doi.org/10.1016/j.jallcom.2016.10.035

[24]	X. Mao, H. Sun, W. Wang, X. Chen, Y. Lu, “Ferromagnetic, ferroelectric properties, and magneto-dielectric effect of Bi4.25La0.75Fe0.5Co0.5Ti3O15 ceramics,” Appl. Phys. Lett., 102, 072904 (2013). https://doi.org/10.1063/1.4793305

[25]	A. K. Kundu, R. Ranjith, V. Pralong, V. Caignaert, B. Raveau, “Magneto-transport and magneto-dielectric effects in Bi-based perovskite manganites,” J. Mater. Chem., 18, 4280–4285 (2008). https://doi.org/10.1039/b806134c

[26]	A. Kumar, K. L. Yadav, “Enhanced magnetodielectric properties of single-phase Bi0.95-xLa0.05LuxFeO3 multiferroic system,” J. Alloys Compd., 554, 138–141 (2013). https://doi.org/10.1016/j.jallcom.2012.11.189

[27]	Y. X. Wang, Y. Ma, Y. Chai, W. Shi, Y. Sun, P. Cheng, “Observation of Magnetodielectric Effect in a Dysprosium-Based Single-Molecule Magnet,” J. Am. Chem. Soc., 140, 7795–7798 (2018).

https://doi.org/10.1021/jacs.8b04818

[28]	N.S. Mukherjee, S. Kashyap, P. Deshmukh, R. Roy, S. Chatterjee, S. Mukherjee, “Negative capacitance and magnetodielectric effect in Cu2O-CuO ceramics,” Ceram. Int., 51, 30716–30722 (2025). https://doi.org/10.1016/j.ceramint.2025.04.264

[29]	P. Yadav, A. Pandey, B. Khan, R. Biswal, A. Fahad, P. Kumar, M.K. Singh, “Detailed investigation on structural, optical, dielectric and magneto-dielectric properties with enhanced magneto-impedance characteristic of NdFeO3 nanoparticles,” Mater. Chem. and Phys., 309, 128424 (2023). https://doi.org/10.1016/j.matchemphys.2023.128424