## Slide 1
Research Center for Materials Nanoarchitectonics (MANA)
Thermal radiation enhancement by thermal extraction of silicon micropyramids
Ryugo Hosokawa1,2, Etsuko Shimada1, Chia-Hung Wu1,3, Satoshi Ishii1,2
E-mail address: hosokawa.ryugo@nims.go.jp
1Optical Nanostructure Team, Nanomaterials Field, MANA, NIMS
2Graduate School of Pure and Applied Sciences, University of Tsukuba
3College of Photonics, National Yang Ming Chiao Tung University
Thermal radiation in air or vacuum
: Thermal radiation intensity
: Stefan–Boltzmann constant
: Temperature of the emitter
: Area of the emitter
Stefan-Boltzman law
Thermal radiation can be enhanced only by increasing the area
Emitter
Emitter
: Thermal radiation intensity
: Stefan–Boltzmann constant
: Temperature of the emitter
: Area of the emitter
: Refractive index of the structure
: Refractive index of the emitter
(if )
(if )
Stefan-Boltzman law
Thermal radiation in high refractive index structures
Absorption
Emitter
Emitter
High refractive index structure
Total internal reflection
Concerns
Solution
Objective
Develop Si pyramid-based thermal extractors
Emitter
Si
Introduction
Experiment
Numerical simulation
Simulation conditions
Magnetic current is used as a thermal radiation source
Wavelength range is 2 - 60 mm, number of pyramids is 7 - 95
Planar Si substrate model and only air model are also calculated
Si pyramids can enhance thermal extraction by 64.6% with the optimized width of 13.2 mm
Si pyramids are useful as thermal extractor, and pyramids have an optimal size for thermal radiation extraction
Applications of thermal radiation
Cooling sheet
https://www.denkishimbun.com/sp/124661
Thermoelectric generation
Ishii, et al, APL (2020)
Proposed structure[1]
Incidence angle of heat on the surface is reduced
Total internal reflection is reduced
Disadvantage
The hemisphere radius needs to be & becomes large
[1] Yu, Z.et al., Nat Commun 2013
Smaller
&
Thinner
Thermal radiation extraction efficiency doesn’t increase with the surface area
Silicon pyramids enhance thermal radiation extraction
The thermal radiation extraction is 25% lower than that of Si hemisphere
There is a pyramid size that can maximize thermal radiation extraction
Heat flux
Si hemisphere > 3 h > 4 h > 2 h > 1 h > 0.5 h > Planar Si
Conclusions
Si pyramid microstructures can reduce light reflection
Si has high refractive index & transparent in the IR region
Experimental and sumerical results showed that Si pyramids perform as efficient thermal extractor
Maximum enhancements of thermal radiation with Si pyramids are **% and ***% in experiment and simulation, respectively
1 hour etched Si pyramid
2 hour etched Si pyramid
3 hour etched Si pyramid
4 hour etched Si pyramid
0.5 hour etched Si pyramid
Schematic of wet etching
Si
NaOH + IPA
Hot plate (80 °C)
Scattering boundary condition
Thermal radiation source | Magnetic current
Wavelength, l | 2 - 60 mm
Number of pyramids | 7 - 95
Air layer radius, r | 100 mm
Si layer height, h | 30 mm
Si layer width, W | 200 mm
Surrounding medium (air)
Silicon substrate
Magnetic current
Simulation model
W
h
r
Integral range of the electric field
: Electric field in the presence of silicon
: Electric field in air
: Blackbody radiation intensity at 300 K
Evaluation of thermal radiation extraction
Finite element method
Electric field norm distribution
Quantified thermal radiation extraction
No Si pyramids
Enhancement factor of Silicon pyramid
Enhancement factor
(No pyramid)
(With pyramid)
Simulation conditions
3 h > 4 h > 2 h > 1 h > 0.5 h > Planar Si > Only emitter
Sample fabrication & SEM images
Peltier module, 5 °C
Doped Si
Si
2 cm
7 cm
Vacuum
P ~ 104 Pa
Al
Heat flow sensor
Vacuum chamber
Measurement setup
Thickness of parts
Emitter
Hemispherical thermal extractor
Enhancement factors of silicon pyramids
Enhancement factor
(With pyramid)
(Planar Si)
Material | Thickness
Si | 500 mm
Al | 100 nm
Doped Si | 500 mm
Sample | Surface area [mm2]
0.5 h | 0.202
1 h | 0.244
2 h | 0.316
3 h | 0.330
4 h | 0.371
Surface areas
*Measurement range
Vertical width: 0.4 mm
Horizontal width: 0.5 mm
Heat flux measurement results
Only emitter