## Slide 1
Figure 1
(b)
(a)
Pores within grain and on boundary
Pores on
triple points
Large defect comprising
agglomerated pores around the unsintered grains
Crack on grain boundary
Frequency
Pore size
Pores within grains
and on boundaries
Pores on
triple points
Pore distribution of possible fracture initiation points
Extreme value side
GP model
Defects comprising agglomerated pores

## Slide 2
Figure 2
(a)
y
z
x
c
R
Pore
Rb
Cracks on grain boundaries
ρ
σF
σF
(b)
XE
YE
XE
NE pores
NE pores
S1
S2
t
W

## Slide 3
(a)
(c)
(b)
× 18
× 18
Total observed area: 12.58 mm2
4.085 mm
3.08 mm
Stress direction
Observed area
Large pore including
unsintered powders
Small pores within grains and on boundaries
50 μm
Figure 3
Crack on grain boundaries
around large defect
Medium pores on triple points

## Slide 4
Figure 4
80 μm

## Slide 5
Figure 5
220.52 µm
214.02 µm
279.85 µm

## Slide 6
(b)
Figure 6
All
Small
Large
Threshold: 5.9 µm
X-Ray CT
All
Small
Large
SEM (SS method)
(a)

## Slide 7
Figure 7
35 μm
0001
(b)
(a)
EBSD
Fitting

## Slide 8
Figure 8
95% Confidence interval
Threshold: 5.9 µm
Linear approximation

## Slide 9
Figure 9
u=5.9 µm
Distribution
A
B
C
ξ [–]
σ [μm]
0.166
3.0
2.3
1.86
X-Ray CT
Distribution A
Distribution B
Distribution C
(b)
(a)
X-Ray CT
Distribution A
Distribution B
Distribution C
Threshold excess of major pore radius
Cumulative frequency H(R – u)

## Slide 10
Figure 10
SEM
Fitting

## Slide 11
Figure 11
Eq. (4)
Distribution A
Distribution B
Distribution C
Exp.
(b)
4pb-L
3pb-L
3pb-S
4pb-S
Exp.
Sim.
2.3 %
97.7 %
he=0.25 mm
(a)

## Slide 12
4pb-L
3pb-L
3pb-S
4pb-S
Exp.
Sim.
2.3 %
97.7 %
he=0.5 mm
Figure 12
4pb-L
3pb-L
3pb-S
4pb-S
Exp.
Sim.
2.3 %
97.7 %
he=0.125 mm
(b)
(a)

## Slide 13
Figure 13
Eq. (4)
0.125 mm
0.25 mm
0.5 mm
Exp.

## Slide 14
Figure 14
0.1 %
1 %
2.3 %
10 %
β
99.9 %
97.7 %
Eq. (4)
Sim. (N=1000)
Exp.
Sim. (N=1000)
Sim. (N=30)
Exp.
(a)
(b)

## Slide 15
Figure 15
Observed data by X-Ray CT
Fitting
Observed data by X-Ray CT
Fitting
(b)
(a)

## Slide 16
Test type | Specimen geometry |  |  | Test geometry | 
Specimen type | t [mm] | w [mm] |  | S1 [mm] | S2 [mm]
3pb-S | 4 | 3 |  | 16 | 0
3pb-L |  |  |  | 30 | 
4pb-S |  |  |  | 30 | 10
4pb-L |  |  |  | 60 | 
Table 1
Table 2
Discretized size he [mm] | ξ [-] | σ [μm] | u [μm] | Pore number [/element] (=ND*he3)
0.125 | 0.166 | 2.3 | 5.9 | 135
0.25 |  |  |  | 1080
0.5 |  |  |  | 8640
Test type | Experiment |  |  | Simulation (Distribution C) | 
Specimen type | m [-] | β [MPa] |  | m [-] | β [MPa]
3pb-S | 14.1 | 412.6 |  | 16.4 | 411.3
3pb-L | 14.5 | 383.9 |  | 16.0 | 387.3
4pb-S | 14.9 | 352.1 |  | 16.2 | 346.2
4pb-L | 18.9 | 338.3 |  | 16.4 | 346.1
Table 3