Surface-modified BaTiO3 as a functional filler in poly(ethylene oxide)-based solid polymer electrolytes for lithium-metal batteries

Shuyu Donga, Yiyi Zhenga, Qiaohui Duana, Yu Zhaoa, Tian Tana, Yu Zhoua, Tian Raoa, Hanbing Yanb, Weiqian Guob, Denis Y. W. Yuc*

aSchool of Energy and Environment, City University of Hong Kong, 83 Tat Chee Avenue, Kowloon, Hong Kong, China

bTsinghua Shenzhen International Graduate School, Tsinghua University, Shenzhen 518055, China

cResearch Center for Energy and Environmental Materials (GREEN), National Institute for Materials Science, Namiki 1-1, Tsukuba, Ibaraki 305-0044, Japan

* Corresponding author

Email: yu.denis@nims.go.jp

Address: Namiki 1-1, Tsukuba, Ibaraki-ken, Japan 305-0044

Figure S1. Schematic diagram of the coating process of BTO@TESPN.

Figure S2. Optical photographs of PEO, BTO@PEO and BTO@TESPN@PEO electrolytes.

Figure S3. Electrochemical impedance plots of a) PEO, b) BTO@PEO, c) BTO@TESPN@PEO electrolytes in stainless steel-stainless steel symmetric cells at 30-60 ℃.

Figure S4. Li-transfer number of PEO and BTO@PEO SPE.

Figure S5. Linear sweep voltammetry plots of PEO, BTO@PEO and BTO@TESPN@PEO electrolytes at a scan rate of 0.1 mV s-1 at 60 C with stainless steel working electrode and Li counter electrode.

Figure S6. Linear sweep voltammograms of Li-Li symmetric cell with PEO, BTO@PEO and BTO@TESPN@PEO electrolytes from -0.25 V to 0.25 V with a scan rate of 1 mV s-1.

Figure S7. Tafel plots and exchange current density of BTO@PEO obtained from the linear sweep voltammetry tests in the range of -0.25 V to 0.25 V

Figure S8. Critical current density of symmetric cells with BTO@PEO electrolytes from a rate-performance test with a capacity of 0.1 mAh cm-2 per half cycle.

Figure S9. Galvanostatic cycling of Li-Li symmetric cell with a) PEO, b) BTO@PEO from 0.1 to 0.4 mA cm-2 with a capacity limit of 0.05 to 0.2 mAh cm-2 (half hour charge/half hour discharge).

Figure S10. Galvanostatic cycling of Li-Li symmetric cell with BTO@PEO electrolytes with 0.1 mA cm-2.

Figure S11. SEM images of Li anode after 10 cycles at 0.1 mA cm-2 /0.1 mAh cm-2 with PEO and BTO@TESPN@PEO electrolytes.

Table S1. Comparison of capacity of PEO-based electrolyte

| Electrolyte compositions | Li+:EO | Specific capacity (mAh g-1) | Cycle number | Capacity retention | Working temperature (℃) | Current density |
| --- | --- | --- | --- | --- | --- | --- |
| PEO+LLZO+SCN[1] | 1:18 | 130.2 | 500 | 80% | 60 | 1.0 C |
| PEO+SN+LiAlO2[2] | 1:10 | 141.3 | 25 | 84.9% | 60 | 1.0 C |
| PEO+LLZTO+SN[3] | 1:18 | 151.1 | 200 | 98% | 60 | 0.5 C |
| PEO+LLZTO@PDA[4] | 1:8 | 142.6 | 50 | 99% | 50 | 0.2 C |
| PEO+PI[5] | 1:15 | 138 | 300 | 96% | 60 | 0.5 C |
| PEO+MOF[6] | 1:18 | 151 | 100 | 95% | 60 | 0.5 C |
| PEO+aligned LAGP[7] | 1:8 | 148.7 | 300 | 93.3% | 60 | 0.3 C |
| PEO+LLZO[8] | 1:16 | 162.7 | 120 | 91.7% | 60 | 0.1 C |
| PEO+KPF6[9] | 1:16 | 142.1 | 200 | 91.3% | 60 | 0.5 C |
| PEO+H2TPP(PEG)4[10] | - | 158.2 | 120 | 97.1% | 60 | 0.2 C |
| PEO+LS-AFE[11] | 1:16 | 112.4 | 150 | 96.7% | 60 | 2.0 C |
| PEO+SBA-LiIL[12] | 1:16 | 150.3 | 90 | 88.4% | 60 | 0.07 C |
| PEO+HPEA[13] | 1:26 | 155.4 | 110 | 90.8% | 50 | 0.1 C |
| PEO+BTO@TESPN (our work) | 1:20 | 155.4 | 700 | 93.0% | 60 | 0.5 C |

References

[1] 	F. Chen, W. Zha, D. Yang, S. Cao, Q. Shen, L. Zhang, D. R. Sadoway, J. Electrochem. Soc. 2018, 165, A3558.

[2] 	N. Zhang, J. He, W. Han, Y. Wang, J. Mater. Sci. 2019, 54, 9603.

[3] 	W. Zha, F. Chen, D. Yang, Q. Shen, L. Zhang, J. Power Sources 2018, 397, 87.

[4] 	Z. Huang, W. Pang, P. Liang, Z. Jin, N. Grundish, Y. Li, C.-A. Wang, J. Mater. Chem. A 2019, 7, 16425.

[5] 	J. Wan, J. Xie, X. Kong, Z. Liu, K. Liu, F. Shi, A. Pei, H. Chen, W. Chen, J. Chen, X. Zhang, L. Zong, J. Wang, L.-Q. Chen, J. Qin, Y. Cui, Nat. Nanotechnol. 2019, 14, 705.

[6] 	J.-F. Wu, X. Guo, J. Mater. Chem. A 2019, 7, 2653.

[7] 	X. Wang, H. Zhai, B. Qie, Q. Cheng, A. Li, J. Borovilas, B. Xu, C. Shi, T. Jin, X. Liao, Y. Li, X. He, S. Du, Y. Fu, M. Dontigny, K. Zaghib, Y. Yang, Nano Energy 2019, 60, 205.

[8] 	Z. Wan, D. Lei, W. Yang, C. Liu, K. Shi, X. Hao, L. Shen, W. Lv, B. Li, Q.-H. Yang, F. Kang, Y.-B. He, Adv. Funct. Mater. 2019, 29, 1805301.

[9] 	J. Li, J. Liang, Z. Ren, C. Shi, Y. Li, L. Zhang, Q. Zhang, C. He, X. Ren, Electrochimica Acta 2022, 429, 141061.

[10] 	Q. Zeng, P. Chen, Z. Li, X. Wen, W. Wen, Y. Liu, H. Zhao, S. Zhang, H. Zhou, L. Zhang, ACS Appl. Mater. Interfaces 2021, 13, 48569.

[11] 	Z. Shi, W. Guo, L. Zhou, Q. Xu, Y. Min, J. Mater. Chem. A 2021, 9, 21057.

[12] 	X. Shen, R. Li, H. Ma, L. Peng, B. Huang, P. Zhang, J. Zhao, Solid State Ion. 2020, 354, 115412.

[13] 	P. Chen, X. Liu, S. Wang, Q. Zeng, Z. Wang, Z. Li, L. Zhang, ACS Appl. Mater. Interfaces 2019, 11, 43146.