## Slide 1
Search for a ferroelectric ice under high pressure
by dielectric and neutron diffraction measurements
using newly developed high-pressure cells
Ryo Yamane (NIMS)
Notes: Thank you chair man for your introduction my name is Ryo yamane belonging to NIMS.
I’m going to talk about ice.
My talking is a little bit difference from the main topic of this session,
but It’s happy for me to give inspirations for your research from my talk.
(20 s)

## Slide 2
Acknowledgement
Komatsu-san
Aoki-san
Prof. Kagi
Prof. Yagi
Iizuka-san
2020 at the University of Tokyo with Kagi’s lab. staffs
Young scientist award 2025
(Japan Society of High Pressure Science and Technology)
(Yesterday’s photo)
Notes: First of all, I’m deeply honored to receive Young scientist award 2025 from Japan Society of High pressure Science and Technology.
I received the prize based on my Ph.D research about ice, and I’d like to express my sincere gratitude to everyone who supported me at Kagi’s Laboratry.
(30 s)

## Slide 3
Water molecules in solids
Vivianite (Fe3(PO4)2･8H2O)
NaxCoO2·yH2O
(x ~ 0.35, y ~ 1.35)
Dehydration induced structural collapse
Water content
Beryl (Be3Al2Si6O18)
Quantum paraelectricity
Superconductivity
The existence of water molecules has great effect on physical properties of host materials.
Ice (H2O)
？
Water molecules exist in many inorganic and organic materials.
Takada et al., (2003)
Gorshunov et al., (2016)
Yamane et al., (2023)
Notes: Water molecule exist many inorganic and organic materials universally.
Some inorganic hydrates and its characteristics derived water molecules are shown here.
The existence of water molecules has great effect on physical properties of host materials.
In this context, physical properties of ice are intriguing as an extreme example case of solids including water molecules.
(30 s)

## Slide 4
Introduction for ice
Water molecules of ice are in hydrogen-bond network
and they have the orientation freedom.
Crystal structure of ice Ih
・Relatively high dielectric constant (ε): ~ 80 - 100
－other hydrated materials also have such high ε ? No.
・Proton conductivity
・Many types of ice polymorphs
－20 crystalline phases have been known.
Next slide
Notes: This is the crystal structure of ice Ih we can find in freezer. Water molecules in ice are in hydrogen-bond network and they have the orientation freedom.
And the orientation freedom of water molecules gives relatively high dielectric constant to ice at around 100.
For your information, other hydrated materials usually don’t show such high dielectric constant; they have 10, typically.
Also the freedom gives proton conductivity which is especially activated at high pressure and high temperature conditions,
And furthermore, one of the reasons of the many types of polymorphs of ice is the freedom of orientation; I will briefly explain this.
(60 s)

## Slide 5
Phase diagram of ice
Disordered ice
Ordered ice
Site occupancy of hydrogen atom: 50%
Site occupancy of hydrogen atom: 100%
50%
100%
O
O
H
H
P (GPa)
T (K)
VII
VIII
VI
XV
XIX
V
XIII
XII
XIV
IX
Ih
XI
II
III
III
V
Ice polymorphs can be classified into disordered and ordered ices.
in
out
…so-called 2-in 2-out (ice rule)
Basic knowledge of ice – disorder-order relationship
Time-space averaged
Disorder-order relationship increases the number of ice polymorphs.
Notes: In phase diagram of ice, we can classify ice polymorphs into disordered and ordered ices, and in each state site occupancy of hydrogen atom is 50 and 100%, respectively.
About the disordered ice the site occupancy is time and space averaged, and in the both state, so called 2-in 2-out or ice rule holds regarding hydrogen positions.
In these states, so called 2-in-2-out or ice rules holds in hydrogen configurations.
And this relationship increase the number of polymorphs
(30 s)

## Slide 6
Many of disorder-order phase transitions of ice need dopants.
Disorder-order phase transitions in hypothetical 2D ice
Hydrogen ordering
Basic knowledge of ice – doping effect
Ice rule restricts the freedom of orientation.
Ice rule holds.
high activation barrier to rotate water molecules
To decrease activation energy
Notes: However it should be noted many of disorder-order phase transitions need dopant.
This is disorder-order phase transitions in hypothetical 2D ice.
As I mentioned, ice rule locally holds in disordered state, and ice rule restricts the freedom of orientation.
and there is high activation barrier to rotate water molecules to transform into ordered state.
So we introduce dopants (such as HCl KOH) to decrease activation energy of the phase transition.
(45 s)

## Slide 7
Crystal structure of ice Ih
・Proton conductivity
・Many types of polymorphs
－20 clystalline phases have been recognized.
Ice shows notable structural and physical properties owing to its hydrogen bond and freedom of orientation on the hydrogen bong network.
・Relatively high dielectric constant (ε)
－other hydrated materials also have high ε ? No.
Research motivation
Ice is the most fundamental hydrogen-bonded molecular material.
Can we control the orientation of water molecules of ice by electric field ? → Ferroelectricity
－Not found yet.
Research motivation:
Very important!!
Notes: Anyway, as I mentioned this molecular dynamics is very important in ice.
And my research motivation is shown here.
Can we control the orientation of water molecules by electric field in ice ? – this means ferroelectricity of ice.
And we have not found yet in bulk ice at least.
For your information, in a kind of organic hydrate ferroelectricity controlled by water contents have been reported.
(45 s)

## Slide 8
Introduction for ice
Ice is the most fundamental hydrogen-bonded molecular material.
Ice shows notable structural and physical properties owing to its hydrogen bond and freedom of orientation on the hydrogen bong network.
Crystal structure of ice Ih
・Relatively high dielectric constant (ε)
－other hydrated materials also have high ε ? No.
・Proton conductivity
・Many types of polymorphs
－20 clystalline phases have been recognized.
Many of ices appear in high pressure, and I expect at least one of them shows ferroelectricity.
Why high pressure?
P (GPa)
T (K)
VII
VIII
VI
XV
XIX
V
XIII
XII
XIV
IX
Ih
XI
II
III
III
V
Notes: And in terms of search for ferroelectric ice, high pressure is very useful tool.
Because many types of ices appear in high pressure region, and I hope at least one of them shows ferroelectricity.
(20 s)

## Slide 9
1. Dielectric measurement (Dynamical information)
2. Neutron diffraction measurement
(Structural information)
To observe
hydrogen atom position
Electric dipole moment
External fields
・High Pressure (HP)
・High-electric field (HE)
To observe water molecule and proton dynamics through each electric response
Measurement methods
Notes: In my research I focused on two measurement methods,
The first one is dielectric measurements. I employed this method “to observe water molecule and proton dynamics through each of electric dipole moment and charge”.
The next one is Neutron diffraction measurements. I employed this method “to observe hydrogen atom position in ice”.
Additionally I combined these measurements with pressure and high electric field.
(30 s)

## Slide 10
My developments
･Pressure can be measured by ruby-fluorescence method.
･Dielectric properties of liquid (or solid) samples can be measured.
((a): the electrodes are self-standing.
(b): the electrodes are immersed in anvils with diamond and epoxy resin.)
･In (c), 10 kV of high voltage is applied.
Characteristics
Piston cylinder
(~ up to 2.5 GPa)
Bridgman anvil cell
(> 10 GPa)
Dielectric
HP-HE neutron diffraction
(Up to 6.1 GPa, 10 kV/mm)
Notes: Let me introduce some my developments,
These developments are for dielectric measurements using two different types of high pressure cells.
This is for HP-HE neutron diffraction measurement up to 6.1 GPa and 10 kV/mm.
As characteristics points, dielectric properties of liquid (or solid) samples can be measured in these cells.
In (a), the electrodes are self-standing. In (b) the electrodes are immersed in diamond and epoxy resin compounds in anvils.
And also pressure can be measured by ruby-fluorescence method in these cells.
In (c), 10 kV of high voltage was applied because of the large sample volume of neutron diffraction measurement.
(70 s)

## Slide 11
Topics
Ice VII under high electric field
Discovery of Ice XIX
Proton-dynamics crossover in ice VII
Notes: In this presentation, I will talk three topics using these developments (10 s)

## Slide 12
Ice VII under high electric field
Notes: First topic is High pressure ice VII under high electric field

## Slide 13
Ice VII （Disordered phase）
Ice VIII （Ordered phase）
Phase diagram of ice
Ice VII appears in a wide pressure range (2 – 60 GPa), and its disordered state has been long investigated.
Liquid
VI
VII
VIII
Short introduction for ice VII
Anti-ferroelectrically
ordered structure
cubic
tetragonal
Notes: Ice VII is a disordered high-pressure phase of ice and its ordered is ice VIII, this is anti-ferroelectrically molecular orientation.
“Ice VII appears … been long investigated”.
(30 s)

## Slide 14
Short introduction for ferroelectrically-ordered form of ice VII
Somayazulu et al., (2008)
14.8 GPa
Intensity (a.u.)
Twotheta (degrees)
They reported a peak splitting of ice VII (for example: 110 reflection).
110
Symmetry lowering (?)
A probability of coexistence of unknown ferroelectrically (FE) ordered form of ice VII has been suggested.
Two proposed ferroelectrically-ordered forms
Caracas and Hemley (2015)
Fukui and Iitaka (2025)
There is a possibility that ice VII cubic lattice is distorted to tetragonal lattice.
HE field can induce?
Notes: Somayazulu et al reported a peak splitting of ice VII at 14.8 GPa,
and this might mean symmetry lowergin of ice VII, and there is a possibility that ice VII cubic lattice is distorted to tetragonal lattice.
From theoretical calculations, A probability of coexistence of unknown ferroelectrically ordered form has been suggested.
(40 s)

## Slide 15
High pressure and high electric field neutron diffraction
Neutron
Incident collimator
(hBN)
n
High voltage
Ground
10 mm
High-pressure cell
Detector
Load
20 mm
(Put behind the press)
Radial collimator (Partitions: Gd2O3)
(at ANSTO, Australia)
HP-HE applying system:
Dr. Helen Maynald-Casely
Dr. Norman Booth
HP-HE cell development:
Yamane (me)
collaborators
Notes: This slide shows the developed high pressure and high electric field neutron diffraction set up.
This study is supported by collaborators, Dr, Helen Maynald-Casely and Norman Booth corresponds to the work of HP-HE applying system,
Dr, Kazuki Komatsu corresponds to the work of collimators.
And I worked for HP-HE cell developments.
This system employs bridgeman anvil type cell and neutron comes from here and detector sets behinds. To decrease parasite scattering we introduces two collimators made of Gd2O3.
And details of cell assembly is explained in next slide.
(60 s)

## Slide 16
HP-HE cell development
High Voltage (10 kV)
Ground
10 mm
n
Anvil (Electrode)
Sample
Gaskets (Pyrophyllite and PTFE)
Cell assembly
Electrodes (anvils) separation is narrowed under high pressure and it is difficult to keep an electrical insulation.
Load
700 ℃, 1 h (Dehydration treatment)
Example of improvements
Developing point
Yamane et al., (2021)
Notes: This is the cell assembly. High voltage is applied to the one of the anvils, the another is connected to ground.
The gasket is composed of the pyrophyllite and PTFE and they also works as insulator.
And, as shown here under high pressure, electrodes (anvils) separation is narrowed and it is difficult to keep an electric insulating.
This is example of gasket improvements, firstly we used row pyrophyllite, but it includes waters in microscale and easily electrical breakdown happens.
Then we heated pyrophyllite to 700℃ to dehydrate water, and as a result, it breakdown voltage had been improved.
(50 s)

## Slide 17
Results – HP-HE neutron diffraction experiments
Expected peak positions from the FE ordered structure
The expected ordered form was not detected even under high-electric field.
Collected at 6.2 GPa
Estimation of volume fraction of the HE-induced polarization
by P-E loop measurement
Notes: This is the result of the experiment.
Unfortunatelly, the expected ordered form was not detected even under high-electric field. These are expected peak positions from the ferroelectrically structure.
Then we estimated volume fraction of the HE-induced polarization.
(30 s)

## Slide 18
Anvil (Tungsten carbide)
Sample
Diamond + Epoxy resin
(mass ratio, 3.8 :1)
Electrode and lead (Cu)
Ruby + plastic fiber
4 mm
Gaskets (SUS + Aluminum)
Another HP-HE cell development
High pressure cell for dielectric measurement was modified.
・Electrodes are immersed in anvils with diamond and epoxy resin.
・Pressure can be estimated by ruby-fluorescence methods.
Ruby-fluorescence system:
Prof. Kentaro Kitagwa
Dr. Takuya Aoyama
acknowledge
Yamane et al., (2021)
Notes: For this purpose, to conduct P-E loop measurement, different high pressure cell for dielectric measurement was modified.
This is the cell assembly, and as I mentioned the electrodes are immersed in diamond and epoxy resin compounds in anvils.
(25 S)

## Slide 19
Anvil (Tungsten carbide)
Sample
Kapton tube
4 mm
Gaskets (SUS + Aluminum)
Newly developed high-pressure cell
HP-HE cell developments
High pressure cell for dielectric measurement was modified.
Cu leads are covered with Kapton tube to prevent electrical breakdown.
→ P-E (polarization-electric field) loop measurements
Notes: When the high voltage is applied in this cell, Cu leads are covered with Kapton tube to prevent electric break down.
(20 s)

## Slide 20
Results and discussion using P-E loop measurements
P-E loop
6.1 GPa
Ice VIII (10 kV/mm, 263 K)
Paraelectric behavior of ice VII was observed up to 10 kV/mm.
Ice VIII （Ordered phase）
Notes: As a result, paraelectric behavior was observed up to 10 kV/mm.
And maximum electric polarization is about 0.8μC/cm2. For your information, when ice VII turns into Ice VIII,
it shows almost 0 electric polarization. This is consistent with the antiferroelectrically configuration.
(30 s)

## Slide 21
Results and discussion using P-E loop measurements
The volume fraction of the FE ordered form was estimated
about 0.02 under 10 kV/mm electric field, if the FE-ordered form coexisted with ice VII.
P = μ(N·f)
Electric polarization
μ : electric dipole moment of water molecule
N: Number of density of water molecules in ice VII
f: Volume fraction of the FE ordered form
6.1 GPa
Ice VIII (10 kV/mm, 263 K)
P-E loop
Notes: And we calculated induced volume fraction of the ferroelectrically ordered form if they induced in ice VII.
Electric polarization can be written by this equation, and also from this structure model
the volume fraction of the ferroelectrically ordered form was estimated about 0.02 under 10 kV/mm electric field, if it coexisted with ice VII.
(30 s)

## Slide 22
Simulation of neutron diffraction pattern
Collected at 6.2 GPa
If 50 kV/mm can be applied to ice VII, the FE-ordered form might be detectable by neutron diffraction → First HE-induced ice phase !?
Electrical breakdown might occur in ice.
P-T-E phase diagram of ice
VII
VIII
E (kV/mm)
?
Notes: This slide shows the neutron diffraction pattern simulation of coexistence of ice VII and the ferroelectrically ordered form.
And under the conditions of the observed 0.02 volume fraction, it was difficult to detect the existence of the ordered form.
And from this simulation if 50 kV/mm can be applied to ice VII, the expected peaks could be observed. This might lead first HE-induced ice phase. But it should be noted that electrical breakdown might occur in ice.
(50 s)

## Slide 23
Proton-dynamics crossover in ice VII
Notes: Next I talk about Proton-dynamics crossover in ice VII briefly.

## Slide 24
Introduction (Proton-dynamics crossover in ice VII)
What is the origin of the disordered state of ice VII ?
Is that unchanged in the wide pressure region 2-60 GPa ?
Rescigno et al., (Nature, 2025)
Plastic ice VII
(~ 5 GPa, 500 K)
wide pressure range
Liquid
Ice VII
T (K)
P (GPa)
Rescigno et al., (Nature, 2025; modified)
This talk focuses on ~RT.
Notes: As I mentioned ice VII appears in the wide pressure range. Very recently plastic ice VII was reported in Nature.
Related to this reports, the disordered state of ice VII has been investigated so far.
And what is the disordered origins of ice VII ?, is that unchanged in the wide pressure region 2-60 GPa ?
(30 s)

## Slide 25
Scenario for proton dynamics in ice VII
A scenario that dominant dynamics of disordered state of ice VII changes from molecular rotation to proton translation.
Molecular rotation
2.9
2.8
2.7
2.6
2.5
2.4
2.3
2.2
2.1
O-O (Å)
103
102
101
O-H…O bond lifetime (fs)
Rotational disorder
Translational disorder
Hernandez and Caracas (2018, modified)
Proton translation (hopping)
High pressure
High temperature
(> 500 K)
Plastic ice VII ? (the rotation is activated)
High pressure (40 – 60 GPa)
Quantum effect appears.
(e.g. Sugimura et al. (2008))
Notes: Hernandez and Caracas suggested from their DFT calculation that dominant dynamics of disordered state of ice VII changes from water rotation into proton translation at around 10 GPa.
In their calculation, they traced each dynamics and evaluated pressure dependence of O-H…O bond lifetime.
The molecular rotation is basic ice molecular dynamics can be also observed in dielectric measurement, and this rotation is activated by temperature, and it is reasonable that plastic ice VII appears.
On the other hand, due to the positive activation volume of the dynamics, the rotation will be weaken with increasing pressure.
And instead, proton translation will be activated with increasing pressure, because of the potential lowering between hydrogen-bonded oxygen atoms.
And further increase, quantum nature will appear.
And I observed the crossover of the dynamics using dielectric measurements.
(90 s)

## Slide 26
Frequency dependence of dielectric relaxations in ice
105
100
10-5
10-10
10-15
Frequency (Hz)
Dielectric constant
(Pettinelli et al., Rev. Geophysics, 2015, modified)
Hopping polarization
Orientational polarization
Ionic polarization
Electronic polarization
Space charge polarization
Molecular rotation
Proton translation
Notes: This is the schematic drawings of the frequency dependence of the dielectric relaxations, and the two dynamics can be observed this region,
and we can detect by dielectric measurement.
and they should shift like this with opposed tendency in frequency.
(30 s)

## Slide 27
Dielectric constant
4.5 GPa
6.2 GPa
7.7 GPa
The two relaxations merged at around 10 GPa.
9.3 GPa
10.5 GPa
Pressure dependence of dielectric relaxations
Frequency (Hz)
100
102
104
10-2
Molecular rotation
102
104
103
102
104
103
102
104
103
102
104
103
102
104
103
Shifts to higher frequency
Shifts to lower frequency
Proton translation
(hopping)
Notes: This slide shows pressure dependence of dielectric constant.
As you can see the higher frequency relaxation shifts to lower frequency region with increasing pressure.
On the other hand lower frequency relaxation shifts to higher frequency region.
And “the two relaxations merge at around 10 GPa”.
(30 s)

## Slide 28
What is the disordered origins of ice VII ?
Is that unchanged in the wide pressure region 2-60 GPa ?
Rescigno et al., (Nature, 2025)
Plastic ice VII
Disordered state transformation
Proton-dynamics crossover in ice VII
Notes: So the disordered state changes from molecular rotation to proton translation at around this region.
Also ice VII remains unresolved problems for example, the bending phase boundaries at around this.
I think ice VII is quite exciting phase.
(30 s)

## Slide 29
Discovery of ice XIX
Notes: This is the last topic of my talk, discovery of ice XIX

## Slide 30
Phase diagram of ice
Before the discovery of ice XIX, one-to-one correspondence held among disordered/ordered ices.
One-to-one correspondence
Disordered
Ih
XI
Ordered
III
IX
V
XIII
VI
XV
VII
VIII
XII
XIV
This study focused on these high-pressure phases, ice VI and XV.
Basic knowledge of ice polymorphism － one-to-one correspondence
Notes: Before the discovery of ice XIX, one-to-one correspondence holds among disordered/ordered ices.
As shown this phase diagram, a disordered ice has its ordered phase, respectively.
And this study focused on these high-pressure phases, ice VI and XV.

## Slide 31
Ice VI
45 hydrogen ordered configurations corresponding to the unit cell of ice VI
1
45
Ice XV (AFE)
The most stable (FE)
Close energy compared to phase-transition temp. (~130 K).
11.3 meV
Ice XV (AFE)
Other hydrogen-ordered configurations
Komatsu et al., (2016)
Energetic degeneracy of hydrogen ordered configurations
45 configurations
Salzman et al., (2009)
Notes: Ice XV is antiferroelectrically ordered structure of ice VI.
Generally, disordered phase has many hydrogen ordered configurations, and there are 45 hydrogen ordered configurations corresponding to the unit cell of ice VI.
Komatsu et al., calculated relative energy of the configurations, and they reported they have close energy compared phase transition temperature between ice VI and XV.
In addition the most stable structure was ferroelectrically ordered configuration.

## Slide 32
Phase diagram of ice
？
？
Multiple hydrogen ordered phases of ice VI ?
Hydrogen ordering of ice VI is slowly and locally occur.
Raman, X-ray, Neutron
Dielectric
Sensitive to detect hydrogen ordering of ice
Piston cylinder know-how:
Prof. Yoshiya Uwatoko
Dr. Jun Gouchi
collaborators
Yamane et al., (2021)
Notes: So, I investigated whether there are more than one hydrogen ordered phases for a disordered phase.
Hydrogen ordered of ice VI is slowly and locally occur, so it is difficult to detect its ordering by typical raman or XRD, nuetron measurement.
Hence I focused on dielectric measurement, it has been known very sensitive to detect hydrogen ordering of ice, using developed piston cylinder cell.
And here I applicate my collaborators Prof. Yoshiya Uwatoko and Dr. Jun Gouchi. They thought me basic piston cylinder know-how.
(80 s)

## Slide 33
H2O with a dopant HCl (concentration：10-2 mol/L)
0.88–2.2 GPa
100–150 K
To accelerate hydrogen ordering of ice VI
Experimental conditions (Dielectric measurements)
P-T condition
Notes: This slide shows experimental conditions for dielectric measurements.
Measured pressure and temperature region is shown here. And I used HCl as a dopant to accelerate hydrogen ordering of ice VI.
(15 s)

## Slide 34
In pure ice VI, the molecular dynamics could not be observed at relatively higher temperature.
Comparison of dielectric properties between pure and doped ice VI
With decreasing temperature,
frequency-dispersion shifts to lower frequency region due to slowdown of the molecular dynamics.
Low temp.
Low temp.
Pure
Doped
Notes: This slide shows comparison between pure and doped dielectric properties of ice VI.
In the both of them, with decreasing temperature, frequency-dispersion shifts to lower frequency region due to slowdown of the molecular dynamics.
And in pure ice VI, the molecular dynamics can not observe by dielectric measurement relatively high temperature.
(30 s)

## Slide 35
Temperature dependence of dielectric relaxation time
The activation energy of the dynamics was decreased by dopant.
pure
doped
Pure
Doped
Comparison of dielectric properties between pure and doped ice VI
Notes: And in this temperature dependence of dielectric relaxation time, the activation energy of the dynamics was decreased by dopant.
(15 s)

## Slide 36
1.9 GPa
150 K
136 K
126 K
122 K
118 K
1 Hz
0.1 Hz
0.01 Hz
Peak disappearance
124 K
Dielectric response decreased at around 124 K.
Temperature dependence of dielectric properties of ice VI and its ordered phase
Notes: Drastic change was observed in the both of dielectric constant and loss data of ice VI at 124 K.
(15 s)

## Slide 37
1.9 GPa
150 K
136 K
126 K
122 K
118 K
124 K
Hydrogen ordering causes a limitation of dynamics of water molecules.
Decreasing of
dielectric constant and loss
(Kawada 1972)
The drastic decreasing of dielectric response can be assigned to hydrogen ordering of ice VI.
Temperature dependence of dielectric properties of ice VI and its ordered phase
Notes: Generally hydrogen ordering causes a limitation of dynamics of water molecules.
This causes decreasing of dielectric constant and loss
The drastic decreasing of dielectric response is assigned to hydrogen ordering of ice VI.
(25 s)

## Slide 38
Ice VI
ΔV > 0
ΔV < 0
A sign of dT/dP changes from negative to positive at around 1.6 GPa.
dT
dP
=
ΔV
ΔS
Clausius-Clapeyron:
(Ordering: ΔS < 0)
Phase diagram of ice VI and its ordered phases
Ice XV
A volume change from ice VI to ice XV is ΔV > 0 (at 0.4 GPa).
(Komatsu et al., 2016)
The unknown ordered phase is in the higher-pressure region.
Notes: Based on the dielectric measurements, I plotted phase transition temperatures in this graph.
As you can see “a sign od dT/dP change from negative to positive at around 1.6 GPa”.
From Clausius-Clapeyron equation, there are two ordered phases which have different volume change comparing with ice VI, because ΔS<0 holds in hydrogen ordering.
Since a volume change from ice VI to ice XV is ΔV > 0, the unknown ordered phase is in the higher-pressure region.

## Slide 39
Experimental conditions (Neutron diffraction)
P-T condition
1.6, 2.2 GPa
80–150 K
D2O with a dopant DCl (concentration：10-2 mol/L)
High-pressure neutron experiment：PLANET(BL11) at J-PARC
Notes: This slide shows experimental conditions for dielectric measurements.
Measured pressure and temperature region is shown here. And I used HCl as a dopant to accelerate hydrogen ordering of ice VI.
(15 s)

## Slide 40
The new ordered phase has unit cell comparing with ice VI.
Ice VI and XV unit cell
New ordered phase unit cell
Diffraction pattern of new phase
（1.6 GPa, 80 K）
HP neutron diffraction experiment
Super lattice reflection
Notes: From time limitation, I do not talk of details of neutron diffraction measurement, but this new phase has √2×√2×1 unit cell comparing with ice VI and XV.

## Slide 41
Based on structural analysis, there are two plausible structure models for ice XIX (Space group: P-4 and Pcc2).
Ice VI and XV unit cell
New ordered phase unit cell
Super lattice reflection
HP neutron diffraction experiment
Diffraction pattern of new phase
（1.6 GPa, 80 K）
Notes: And there are two plausible structure models for ice XIX whose space group are P-4 and Pcc2, respectively.

## Slide 42
(Fully ordering could not be observed by dielectric measurements.)
Remains problems of ice XIX
・Are there fully hydrogen ordered phases ?
Site occupancy of D3 (hydrogen) positions are identically 0.5. Pcc2 (and also P-4) structure models indicate ice XIX is partially ordered phase.
Pcc2
・Which space group is correct ?
・How ice XIX responses under high electric field ?

## Slide 43
Summary
Not only for ice,
High pressure × High electric field
is a frontier research region !
thank you for listening !
Notes: As a summary, I focused on the molecular dynamics of ice, and I developed high pressure cells.
And using them, I studied high pressure ices to search ferroelectric ice.
Not only in hydrates but also water is important solvent in chemical reactions and crystal growth,
so I believe the high pressure developments has great potential in wide scientific field, thank you!

## Slide 44
Supporting information

## Slide 45
Dielectric constant and loss
Dielectric constant
Dielectric loss
Frequency (Hz)
Previous study (e.g. Yamane et al., 2017)
・The higher frequency relaxation is assigned to a molecular rotation in previous studies.
？
Lower frequency relaxation
Loss peak
・Two clear dielectric relaxations were observed.
10-1
100
101
102
104
103
105
10-2
104
105
106
Frequency (Hz)
120
100
80
60
40
20
0
Dielectric constant and loss
102
104
103
105
102
104
103
101
101
Higher frequency relaxation
Results at 5.4 GPa
Notes: This slide shows results at 5.4 GPa, and the left side shows dielectric constant and loss.
As you can see, we observed two clear dielectric relaxations.
Higher frequency relaxation is assigned to water rotation in previous studies as I mentioned after.
In dielectric loss data, the higher frequency relaxation has loss peak. But the lower frequency relaxation seems to not have a loss peak.
In much lower frequency region, another relaxation was observed and this is derived between sample and electrode and generally
this dielectric relaxation cause larger dielectric loss as you can see here.
So I think loss peak derive from lower relaxation might be hidden.
(60 s)