Cumulative effect of spectral downshifting, anti-reflection and space charge region formation in enhancing the spectral response of Self-powered Silicon photodetector on sensitisation with CdZnS/ZnS Core-shell Quantum dots

Kumaar Swamy Reddy Bapathi abc, Mostafa F. Abdelbar cd, Wipakorn Jevasuwan c,

Pramod H Borse b, Sushmee Badhulika a*  and Naoki Fukata c*

a Department of Electrical Engineering, Indian Institute of Technology Hyderabad, Kandi, Sangareddy, Hyderabad

b Centre for Solar Energy Materials, International Advanced Research Centre for Powder

Metallurgy & New Materials, Balapur, Hyderabad

c Research Centre for Materials Nanoarchitectonics, National Institute for Materials Science, Tsukuba, Japan

d Institute of Nanoscience & Nanotechnology, Kafrelsheikh University, 33516 Kafrelsheikh, Egypt

Figure S1. Quantum dots particle size distribution

Figure S2. EDS spectrum of CdZnS/ZnS core-shell quantum dots.

Figure S3. CdZnS/ZnS quantum dots under a) Ambient light and b) UV illumination

Figure S4. SEM images of Pristine Silicon and CdZnS/ZnS QD films deposited films deposited on Silicon. a) Pristine Silcon b) 1 Layer QDs, c) 2 Layer QDs, d) 3 Layer QDs, e) 4 Layer QDs and f) 5 Layer QDs.

Figure S5. Temporal response of the detector under varied light intensities (0.1 – 2 mW/cm2 a) 300 nm, b) 600 nm, and c) 820 nm

Figure S6. I-V characteristics of Control Si devices with a) Ti-Ag and b) Ag electrodes

Figure S7. Photocyclic stability of CdZnS/ZnS QD- Si photodetector under a) 320 nm, b) 600 nm and, c) 900 nm

| Materials | Synthesis/ Fabrication technique | Architecture | Spectral Response | Bias | Responsivity | Rise Time | Detectivity | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PbSe QDs | Hot Injection and Spin Coating | Au-(Si - ZnO-PbSe QD)-Au | 808 nm | 1V | 100 mA/W | 340 ms | 1.86 × 1011 Jones | 1 |
| SiNWs-Carbon QDs | Electrochemical Etching and Spin coating | In/Ga – (n-SiNW – Carob QDs) - Au | 300-1100 nm | 0V | 350 mA/W | 20 µs | 3.79 × 109 | 2 |
| Si- Carbon QDs | Hydrothermal and Drop coating | Al/Si/C-QDs/Ag | 352—850 nm | 0V | 9.4 mA/W | 10 µs | 5.9 × 1012 | 3 |
| MoS2-CuInS2 QDs-AuNPs | Hot injection and spin coating | Au- ( MoS2-CuInS2-AuNPs) -Au | 405 – 635 nm | 4V | 16.65 mA/W | 5s | 2.2 x 1012 | 4 |
| SWCNT-PbSQDs-MAPbX3 | Hot injection and dip coating | ITO –( SWCNT-PbSQDs-MAPbX3)- ITO | 30-1500 nm | 1V | 500 mA/W | 250 µs | 1.4 × 1011 Jones | 5 |
| MXene/CsPbBr3 | Hot injection and spin coating | Au - ( MXene/CsPbBr3) - Au | 300-550 nm | 1V | 0.1 mA/W | 48.2 ms | 108 | 6 |
| AgAuSe QDs | Hot injection and spin coating | Au – AgAuSe-Au | 808 nm | 0V | 0.35 mA/W | 3.1 s | 1.55 × 1010 Jones | 7 |
| CsPbBr3 (SbBr3) | Hydrothermal and Drop coating | FTO-CsPbBr3-Al | 405 nm | 0V | 0.048 mA/W | 98 ms | No data | 8 |
| Si-PbS QDs | Hot injection and spin coating | Ti/Pt/Au-P-Si-SiNx-(PbS-TBAI)-ITO | 1064 nm | 0V | 250 mA/W | 20 µs | 7.74 × 1010 | 9 |
| Si - CdZnS/ZnS core-shell QDs | Hydrothermal and Drop coating | Ti/Ag – Si – CdZnS/ZnS - Ag | 300- 1100 nm | 0V | 350 mA/W | 82 ms | 2.89 x 1012 | This Work |

Table S1. Comparison of our fabricated CdZnS/ZnS QD-Si device with other QD based detectors.

(1)	Peng, M.; Liu, Y.; Li, F.; Hong, X.; Liu, Y.; Wen, Z.; Liu, Z.; Ma, W.; Sun, X. Room-Temperature Direct Synthesis of PbSe Quantum Dot Inks for High-Detectivity Near-Infrared Photodetectors. ACS Appl. Mater. Interfaces 2021, 13 (43), 51198–51204. https://doi.org/10.1021/acsami.1c13723.

(2)	Xie, C.; Nie, B.; Zeng, L.; Liang, F.-X.; Wang, M.-Z.; Luo, L.; Feng, M.; Yu, Y.; Wu, C.-Y.; Wu, Y.; Yu, S.-H. Core–Shell Heterojunction of Silicon Nanowire Arrays and Carbon Quantum Dots for Photovoltaic Devices and Self-Driven Photodetectors. ACS Nano 2014, 8 (4), 4015–4022. https://doi.org/10.1021/nn501001j.

(3)	Hsiao, P.-H.; Kuo, K.-Y.; Chen, Y.; Wu, T.-Y.; Chen, C.-Y. Balance of Photon Management and Charge Collection from Carbon-Quantum-Dot Layers as Self-Powered Broadband Photodetectors. Nanoscale Adv. 2023, 5 (4), 1086–1094. https://doi.org/10.1039/D2NA00852A.

(4)	Qin, S.; Li, K.; Zhu, J.; Xu, H.; Ali, N.; Rahimi-Iman, A.; Wu, H. A New Strategy to Improve the Performance of MoS2-Based 2D Photodetector by Synergism of Colloidal CuInS2 Quantum Dots and Surface Plasma Resonance of Noble Metal Nanoparticles. J. Alloys Compd. 2021, 856, 158179. https://doi.org/10.1016/j.jallcom.2020.158179.

(5)	Ka, I.; Gerlein, L. F.; Asuo, I. M.; Nechache, R.; Cloutier, S. G. An Ultra-Broadband Perovskite-PbS Quantum Dot Sensitized Carbon Nanotube Photodetector. Nanoscale 2018, 10 (19), 9044–9052. https://doi.org/10.1039/C7NR08608C.

(6)	Li, H.; Li, Z.; Liu, S.; Li, M.; Wen, X.; Lee, J.; Lin, S.; Li, M.-Y.; Lu, H. High Performance Hybrid MXene Nanosheet/CsPbBr3 Quantum Dot Photodetectors with an Excellent Stability. J. Alloys Compd. 2022, 895, 162570. https://doi.org/10.1016/j.jallcom.2021.162570.

(7)	Wang, Z.; Liu, F.; Gu, Y.; Hu, Y.; Wu, W. Solution-Processed Self-Powered near-Infrared Photodetectors of Toxic Heavy Metal-Free AgAuSe Colloidal Quantum Dots. J. Mater. Chem. C 2022, 10 (3), 1097–1104. https://doi.org/10.1039/D1TC03837K.

(8)	Subramaniam, M. R.; Pramod, A. K.; Hevia, S. A.; Batabyal, S. K. Enhanced Photoluminescence Quantum Yield, Lifetime, and Photodetector Responsivity of CsPbBr3 Quantum Dots via Antimony Tribromide Post-Treatment. J. Phys. Chem. C 2022, 126 (3), 1462–1470. https://doi.org/10.1021/acs.jpcc.1c07493.

(9)	Wang, J.; Chen, J. High-Sensitivity Silicon: PbS Quantum Dot Heterojunction near-Infrared Photodetector. Surf. Interfaces 2022, 30, 101945. https://doi.org/10.1016/j.surfin.2022.101945.