Effect of Oxygen Terminal Surface Adsorption Layer on Energy Dissipation in Single-Crystal Diamond MEMS
National Institute for Materials Science 1, Shanghai University 2, Tohoko University 3
○ (DC)Keyun Gu 1,2, Zilong Zhang 3, Wen Zhao1, Guo Chen 1, Jian Huang 2, Satoshi Koizumi 1, 
Yasuo Koide 1, and Meiyong Liao 1
E-mail: meiyong.liao@nimg.go.jp

[image: image1.wmf]300

400

500

600

700

800

900

804.36

804.38

804.40

804.42

 L: 80 

µ

m

Frequency (kHz)

?

?

?

Processing temperature (K)

Test at RT

(a)

(

b

)

 Single-crystal diamond (SCD) presents as a promising candidate for the achievement of low mechanical dissipation or high quality (Q) factors for high-sensitivity and high signal-to-noise (SNR) ratio microelectromechanical systems (MEMS) sensors by virtue of its outstanding mechanical characteristic, high thermal conductivity, excellent electronic properties, and the characteristics of non-grain boundary and non-impurity phase [1-3]. The SCD MEMS resonators were fabricated by Ion implantation-assisted smart-cut technique [4,5]. The effect of the ion-irradiation induced defective layer has been minimized and the Q factor has been achieved over one million through atomic etching [6]. Nevertheless, how the surface terminal adsorption characteristics of diamond affects the Q factors of SCD MEMS is still mysterious. Therefore, the clarification of the oxygen-termination effect is critical to achieve the ultra-high Q factor MEMS resonators.
    In this work, we clarify the effect of oxygen terminal surface adsorption characteristic on the resonance behavior of SCD MEMS resonator. We examine the Q factors and resonance frequencies of the SCD MEMS resonators with the defective layer removed in a high vacuum chamber by in-situ heating and cooling. Based on ultrahigh stability of resonance characteristic of SCD resonator at room temperature (RT) and high temperature (from 313 K to 933 K), the Q factors are significantly improved after heating processing. The Q factor of the 80 μm-long cantilever is improved from 1.0x105 to 1.2x105 and the resonance frequency increases, as shown in Fig.1. We clarify that the desorption of the absorbates on the oxygen-terminated diamond surface induces the lower surface energy dissipation and higher Q factor. Hence, appropriate surface treatments are necessary for the development of MEMS devices with low energy dissipation and high sensitivity.
References: [1] H. Sun, et al., Adv. Quantum. Technol. 2300189 (2023). [2] Z. Zhang, et al., Mater. Res. Lett. 8, 180-186 (2020). [3] Z. Zhang, et al., ACS Appl. Mater. Interfaces 12, 23155-23164 (2020). [4] M. Liao, et al., Adv. Mater. Technol., 4, 1800325, 2019. [5] M. Liao, et al., Adv. Mat. 22, 5393 (2010). [6] H. Wu, et al., Carbon 124, 281-287 (2017). 
�





Figure 1. The resonance frequency and the Q factor of the 80 μm-long cantilever measured at RT after cooling back from different high temperatures.








