Low-energy Dissipation Diamond MEMS

Guo Chena,b, Satoshi Koizumia, Yasuo Koidea, Meiyong Liaoa*

a Research Center for Electronic and Optical Materials, National Institute for Materials Science, 1-1 Namiki, Tsukuba, Ibaraki 305-0044, Japan

bChina University of Geosciences (Beijing), No.29, Xueyuan Road, Haidian District, 100083, Beijing, P.R. China

E-mail: meiyong.liao@nims.go.jp

# CONSPECTUS

The microelectromechanical systems (MEMS) that integrate tiny mechanical devices with electronics on a semiconductor substate has experienced explosive growth over the past decades. MEMS have a range of wide applications from accelerometers and gyroscopes in automotive safety, to precise reference oscillators in consumer electrons to probes in atomic force microscopy and sensors for gravitational wave detection. Quality (Q) factor is a fundamental parameter of a MEMS resonator that determines the sensitivity, noise level, energy efficiency, and stability of the device. MEMS with low energy dissipation has always been pursued. Despite the brilliant progress of silicon-based MEMS due to the mature technology in counterpart microelectronic, the intrinsic material properties limit the sensitivity and reliability, especially for the applications under extreme conditions. Diamond has emerged as the ideal semiconductor material for low-energy dissipation MEMS with high-performance and high-reliability, owing to its unparalleled material properties, such as the extremely high mechanical strength, super electrical properties, the highest thermal conductivity, and chemical inertness. Diamond resonators are thus expected to exhibit high Q-factors, and high reliability, with low thermomechanical force noise and long coherence rate of mechanical quantum states, not only improving the performance of MEMS devices but also expanding to the quantum domain. Single-crystal diamond (SCD) is desirable to achieve the ultra-low energy loss or high Q-factor MEMS resonator due to non-existence of grain boundaries and other carbon phases. However, the micromachining for SCD is tough and heteroepitaxial growth of SCD on foreign substrates remains quite difficult.

In this Account, we provide an overview of the recent research and strategies in SCD diamond MEMS for achieving high Q-factors, focusing on those fabricated by the smart-cut method developed in our lab. We start with the concept of diamond MEMS, covering from structures fabrication, fundamentals, to applications. A comprehensive discussion of the energy dissipation mechanisms on the Q-factors in diamond MEMS resonators is provided. The approaches to enhance the Q-factor of diamond resonators including (1) the growth of high crystal quality SCD epilayer on the ion-implanted substrate, (2) defects engineering, and (3) strain engineering by thinning the resonator to around 100 nm thick are presented. In the smart-cut method, the ~100 nm thick defective layer contributes to the main intrinsic energy loss. By combing the growth of a high crystal quality diamond epilayer above the defective layer and the atomic scale etching of the defective layer, the Q-factors could be improved from thousands to over one million at room temperature, the highest among all the semiconductors. The intrinsic high Q-factors of SCD MEMS is also due to the well-controlled purity of the diamond epilayer and the ultra-wide bandgap energy of diamond. Through strain engineering of the SCD MEMS beam to nanoscale, the Q-factor is expected to be further enhanced.  These strategies represent pivotal steps in advancing the performance and applicability of diamond MEMS resonators.

# 1. INTRODUCTION

Microelectromechanical systems (MEMS) and nanoelectromechanical systems (NEMS) stand out as a cutting-edge multidisciplinary field based on the interaction between electrical and mechanical components. MEMS devices offer promising applications in automation, industry, edge computing, augmented/virtual reality, biomedicine, telecommunications, and quantum mechanics, because of their advantages of smaller, faster, more sensitive, integrability, and low power consumption.1, 2 The past decades have witnessed explosive growth of silicon-based MEMS due to the compatibility with the mature complementary metal-oxide-semiconductor (CMOS) industry. High-frequency and high-quality (Q) factor or low dissipation (or loss) as well as high-reliability MEMS/NEMS resonators have been pursued for better devices properties, such as high sensitivity, high resolution, strong robustness to heat and radiation, and resilience against wear and mechanical attack, as the development of health care for human being, artificial intelligence, autonomous driving, smart robots and space exploration.3 Nevertheless, due to the intrinsic material limitations of silicon such as the narrow bandgap energy, surface native oxidation, and mechanical brittleness, especially when the dimensions entering nanoscale, the performance such as the sensitivity and reliability of the current MEMS devices have been facing bottlenecks. Diamond with an ultra-wide bandgap (UWBG) of 5.5 eV has proven to be an ideal material to overcome the drawbacks of the conventional MEMS/NEMS, especially for the applications in harsh environments, due to its superior mechanical properties, high thermal conductivity, hydrophobic surface, chemical inertness, biocompatibility, and low intrinsic dissipation.4-6

The advancement of diamond MEMS/NEMS resonators is critically dependent on the micromachining fabrication of the freestanding structures, such as cantilever beams, bridges, disks, and membranes, etc. Methods for fabricating PCD/NCD diamond micro-resonators had been realized based on the micromachining the silicon substrate or selective growth, which have the merits of large area production.7, 8 Several prototypes PCD/NCD MEMS devices such as pressure sensors and GHz resonators were demonstrated.9, 10 Nevertheless, the grain boundaries and other carbon phases induce inter-friction limit the ultimate devices performance. Diamond MEMS/NEMS have been used in many different applications, including magnetic sensors, radio frequency (RF) switches, actuators, and atomic force microscope (AFM) probes.11, 12

Mainly, the fabrication techniques of SCD MEMS/NEMS resonators include smart-cut method based on the ion-implantation assisted lift-off (IAL)13-15, angled anisotropic plasma etching (APE)16, 17, and 1(DOI) methods18-20. Over the past decade, our group has been developing SCD MEMS/NEMS with a structure of diamond-on-diamond using the smart-cut method with well-controlled device dimensions. We demonstrated SCD NEMS switches13, 21 and high-temperature SCD MEMS magnetic sensors11, 22-24. Nevertheless, the ion-implantation in the smart-cut method introduce damages to a semiconductor crystal, degrading the Q-factor of SCD cantilevers to several thousand, orders of far below those expected. Figure 1 provides an overview of high Q-factor and high frequency diamond MEMS/NEMS, including fabrication techniques and representative applications. In total, the low-energy dissipation of diamond provides resonators with ultra-high Q-factors, making it ideal for developing ultrahigh-performance and robust MEMS in sensing and quantum science fields. This capability surpasses that of other semiconductors. For instance, we achieved high self-sensitivity (3.2 Hz mT−1 at 500°C) and low noise level (9.45 nT Hz−1/2 at 300°C) in an on-chip SCD MEMS magnetic sensor by improving the Q-factor11. This work highlights how diamond’s low-energy dissipation enhances Q-factors, facilitating the development of diamond MEMS sensors with unparalleled reliability, particularly in challenging environments such as high temperatures.

In this Account, we firstly provide insight into the energy dissipation mechanisms in SCD MEMS/NEMS. Then, we show the strategies for achieving high Q-factors resonators that include: (1) improving the overall crystal quality of the resonator; (2) defects engineering through either point defects annihilation or surface etching defects in diamond resonators; and (3) strain engineering. Finally, a conclusion and outlook are presented.

- Figure 1. An overview of diamond MEMS/NEMS. Typical fabrication methods for high Q-factor and high frequency diamond MEMS/NEMS to achieve high performance and high reliability in diverse applications. Reproduced with permission from reference 11. Copyright 2023 Wiley-VCH GmbH. Reproduced with permission from reference 13. Copyright 2010 Wiley-VCH Verlag GmbH & Co. KGaA, Weinheim. Reproduced with permission from reference 16. Copyright 2012 American Chemical Society. Reproduced with permission from reference 18. Copyright 2013 WILEY-VCH Verlag GmbH & Co. KGaA, Weinheim. Reproduced with permission from reference 25. Copyright 2021 AIP Publishing. Reproduced with permission from reference 26. Copyright 2018 Elsevier B.V. Reproduced with permission from reference 27. Copyright 2021 The Japan Society of Applied Physics.

# 2. ENERGY DISSIPATIONS IN DIAMOND MEMS/NEMS

## 2.1 Q-factor and Resonance Frequency

The dissipation of a mechanical resonator is the energy loss rate of a mode of resonance, which can be expressed by the reciprocal of Q-factor of Q−1. The Q-factor and the resonant frequency (fr) define the basic properties of a mechanical resonator.28 Low dissipation or high Q-factor has always been pursued. The Q-factor ultimately determines the sensitivity of the device response, such as to force, mass, displacement, etc. For instance, the minimal detectable force (Fmin) for a simple rectangular cantilever is given by29

| Fmin= wt2LQ1/2kBTB1/2Eρ1/4 | (1) |
| --- | --- |

where E and ρ note Young’s modulus and mass density of the cantilever material; B notes the bandwidth of the system; w, L, and t represent the cantilever dimensions in width, length, and thickness respectively. The Q-factor is typically calculated from the full-width at half maximum (FWHM, ∆f) of the resonance spectrum obtained by fitting Lorentzian shapes, defined as30

| Q-1=ΔW2πW0≈ ∆ff | (2) |
| --- | --- |

Here, W0 represents the total mechanical energy, ΔW represents the energy dissipated per cycle of oscillation, and f represents the resonance frequency.

The resonance frequency of a cantilever can be described by the classic Euler-Bernoulli theory as the follow31

| f= ktL2Eρ | (3) |
| --- | --- |

where k represents a resonance mode-dependent constant, typically 0.162 for a cantilever in the first order of the out-of-plane resonance mode. Achieving a higher resonant frequency requires reducing dimensions. However, miniaturization beyond the submicron scale results in increased dissipation.3

## 2.2 Energy Dissipations in Diamond MEMS/NEMS

To achieve high-performance, high-reliability, and energy-saving diamond MEMS/NEMS devices, understanding the energy dissipation mechanisms is of great significance. The intricate relationship between the Q-factors and the geometric dimensions implies the presence of diverse sources of dissipation.32 Usually, we consider the primary dissipations while ignoring the others in order to better understand the energy dissipation mechanism. The entire Q-factor for a MEMS resonator with a given resonant frequency can be written as the sum of all dissipations:

| 1Q= 1Qair+ 1Qclamp+ 1QTED+ 1QMD+ 1Qsurface | (4) |
| --- | --- |

where the Q-factors for the dissipation sources from air damping, clamping/support loss, thermoelastic damping (TED), mechanical defects (MD), and surface loss are represented by Qair, Qclamp, QTED, QMD, and Qsurface, respectively. We investigated the dominated dissipation mechanism by excluding other mechanisms one by one.

(1) Air Damping

In practice, MEMS/NEMS devices are usually operated in atmospheric or low vacuum environments. Investigating the air dampening effect and how ambient gas pressure affects diamond cantilever Q-factor is necessary. The ambient pressure in the range of 10-3 to 105 Pa can be classified into intrinsic (P < 10 Pa), molecular (10 Pa < P < 103 Pa), and viscous (P > 103 Pa) regimes by Knudsen number.33 Following that, the overall damping, which includes viscous, molecular, and intrinsic damping, is represented as follows

| 1Qtotal= 1Qintrinsic+ 1Qmolecular+ 1Qviscous | (5) |
| --- | --- |

In the intrinsic regime, air damping exerts a negligible influence since the mean free path of molecules greatly exceeds the dimensions of the diamond cantilever. The dissipation mechanism in the molecular regime combines the effects of both the intrinsic and viscous regimes. The following two models34 can be used to fit experimental data for Qmolecular:

| Qmolecular, Chr= ρtfn4∙π2∙R0TMm∙1P | (6) |
| --- | --- |
| Qmolecular,Bao= π232∙R0TMmP∙tρfn | (7) |

Here, ρ represents the specific mass of diamond (3,500 kg/m), t and fn represent the thickness and the resonance frequency of cantilever, R0 represents the gas constant (8.317 J/(mol K)), T denotes the absolute temperature during measurement (K), Mm represents the molar mass (29 g/mol for air), P stands for the ambient pressure. Thus, Qmolecular is inversely proportional to P. In the viscous regime, the Qviscous can be expressed as34

| Qviscous= 2ρW2fn6πμW+32πW22μMmRTfnP | (8) |
| --- | --- |

where μ denotes the dynamic viscosity of air, which is 1.85 × 10−5 kg/(m s), W is the cantilever width. Hence, Qviscous is predominantly influenced by P1/2. The air damping dominates the energy Q-factors of the SCD cantilevers in air, leading to the value to ~100 for the first out-of-plane resonance mode.34

(2) Clamping Loss

When the measurement is made in a vacuum (less than 10-5 Pa) at room temperature, the air damping and TED can be excluded. Both MD and surface loss mechanisms are independent of cantilever dimensions. Thus, the dominant energy dissipation for the SCD cantilevers with shorter lengths was attributed to clamping loss. Two models were considered for describing the clamping loss of out-of-plane flexural cantilevers. The Q-factor resulting from clamping loss for an infinite-width cantilever fixed to a semi-infinite base can be written as35, 36

| Qclamp= αLt3 | (9) |
| --- | --- |

where α is a constant. A different flexural cantilever model with a finite base was put forth as37

| Qclamp= βLwtbt2 | (10) |
| --- | --- |

where tb is the base thickness and β is a constant.

(3) Thermoelastic Damping

Thermoelastic damping stands as an important energy dissipation mechanism resulting from heat conduction during the transverse vibration of cantilevers, which can be estimated as38

| QTED-1= α2TEρCp2fnρCpt2πk1+2fnρCpt2πk2 | (11) |
| --- | --- |

where α, T, Cp and k respectively denote the linear expansion coefficient, environment temperature, heat capacity and thermal conductivity of the cantilever material. TED only becomes dominant at high temperatures for perfect SCD cantilevers.

(4) Mechanical Defects

The dissipation resulting from mechanical defects (MD) in the mechanics is written as follows39,

| QMD-1= δωτMD1+ωτMD2 | (12) |
| --- | --- |
| τMD= τMD0-1exp-EAkBT | (13) |

where ω signifies the resonance frequency, τMD signifies the defect relaxation time, and δ is a unitless constant associated with defect concentration. The characteristic atomic vibration period, τMD0, is approximately 10-13 s. The defect’s activation energy is represented as EA. A Debye peak is produced when the mechanical defect dissipation reaches its maximum at ωτMD = 1.

The ultrawide band gap of diamond sets it apart from other semiconductors since all known defects possess deep energy levels that exhibit low activity at room temperature. We explored the effect of deep defects on the mechanical energy dissipation of diamond resonators after removing the ion-radiation reduced layer across a temperature range from room temperature (RT) to 973 K. To exclude other effect for energy dissipation, the temperature-dependent resonance frequency was investigated. Figure 2(a) displays the temperature dependence on the resonance frequency of a 120 μm-long diamond cantilever.39 The temperature-dependent resonance frequency was examined to extract the Young’s modulus as a function of temperature for subsequent energy dissipation analysis. The temperature-dependent Young’s modulus models the exponential drop in resonance frequency with temperature40,

| ET= E0-CTexp-T0T | (14) |
| --- | --- |

where E0 represent the Young’s modulus at 0 K, C is a constant that is independent of temperature, and T0 is a characteristic temperature that is connected to the SCD Debye

temperature with the formula of T0 = ϴD/2. The decrease in the SCD cantilever’s Young’s modulus is responsible for the resonance frequencies’ nonlinear downward trend as temperature rises.

Figure 2(b) shows the temperature dependence of Q-factor from RT to 973 K for the same cantilever as in Figure 2(a). The Q-factors exceed 10,000 across the entire temperature range, with a maximum value approaching 200,000 near 400 K. It is observed that, on average, the Q-factor decreases with increasing temperature, with two maxima observed near 400 K and 900 K. Based on the temperature-dependent Q-factors, we inferred the presence of two types of mechanical defects in this case. We used the following equation as our model,3, 31

| Qtotal-1= Qclamp-1+ Qsurface-1+ QTED-1+ QMD1-1+ QMD2-1 | (15) |
| --- | --- |

By simulating each energy dissipation source in Equation (15) as done in Figure 2(c), we derived the total Q-factors, illustrated in Figure 2(d). It is observed that the energy dissipation increases with temperature and shows local maxima because of the interplay between deep defects that are triggered at specific temperatures and phonons. Removing boron impurities notably enhances the Q-factor of RT diamond resonators. The deep energy nature of these defects provides SCD with remarkably low intrinsic energy dissipation in mechanical resonators, at RT and even beyond.

- Figure 2. The measured resonance frequencies (a) and Q-factors (b) of cantilevers with length of 120 μm as a function of temperature ranging from RT to 700°C (973 K). (c) Temperature-dependent variations in each dissipation source. MD1 represents the mechanical dissipation associated with defect D1, while the dissipation related to defect D2 is absent and thus not depicted. Here, δ1 equals 10−4 and δ2 equals 0. (d) Plot of calculated Q-factors versus temperature for various defect concentrations, distinguishing between the activation of each type of defect: Red lines depict D1 with an excitation energy of 0.33 eV, while blue lines represent D2 with an excitation energy of 0.91 eV. Reproduced with permission from reference 39. Copyright 2020 American Physics Society.

(5) Surface Loss

For the surface loss, it’s primarily caused by surface states, that can be significantly influenced by surface oxides, absorbates and defects. The surface loss can be mathematically represented as3, 41

| Qsurface-1= 2δ3ω+tωtE1SE | (16) |
| --- | --- |

Here, δ is the thickness of the surface layer where E1S is defined. A merit of diamond for MEMS is that there is no existence of solid native oxides on the surface.  In our work, surface loss can be included in the mechanical defect loss due to ion-implantation induced defective layer at the bottom of the SCD cantilevers.

# 3. TACTICS TO REDUCE DISSIPATION FOR HIGH Q-FACTOR

## 3.1 Improve Overall Resonator Crystal Quality

The crystal quality determines the intrinsic energy dissipation in SCD MEMS. PCD and N/UNCD often exhibit a high-volume fraction of grain boundaries and impurities due to their smaller crystal sizes, degrading the Q-factors7 (see Table 1 and 2). The development of MEMS/NEMS devices using SCD becomes highly desirable, as it allows for the exploitation of diamond’s extraordinary properties in the realm of MEMS/NEMS technology.42 Additionally, the Q-factor of electronic-grade SCD (el-SCD) surpasses that of optical-grade SCD.

Table 1. Q-factors and Raman FWHM for Different Diamond Cantilevers

| Material | Length | Width | Thickness | FWHM of Raman | Q-factor | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| SCD | 100 µm | 12 µm | 1.5 µm | 2.8 cm-1 | 30,000 | 43 |
| SCD | 100 µm | - | 1.4 µm | 2.4 cm-1 | 13,000 | 44 |
| SCD | 100 µm | 10 µm | 1 µm | 1.8 cm-1 | 8,000 | 45 |
| SCD | 100 µm | - | - | 1.75 cm-1 | 20,000 | 46 |
| el-SCD | 240 µm | 12 µm | 660 nm | - | 412,000 | 19 |
| PCD | 200 µm | 18 µm | 270 nm | - | 6,680 | 19 |
| NCD | 500 nm | 300 nm | 600 nm | - | 4,380 | 47 |
| UNCD | 200 µm | 27 µm | 1 µm | - | 10,000 | 48 |

Table 2. Q-factors of Typical MEMS Based on Different Materials

| Material | Resonator | f | Q-factor | Temperature | Ref. |
| --- | --- | --- | --- | --- | --- |
| SCD | cantilever | 214 kHz | 1,006,178 | 300 K | 43 |
| Si | cantilever | 495 kHz | 22,500 | 4.2 K | 49 |
| SiO2/TiO2 | beam | 278 kHz | 9,000 | 295 K | 50 |
| SiN | beam | 8.07 MHz | 10,000 | 300 K | 51 |

The Q-factors of diamond resonators fabricated through the IAL technique are significantly lower than those fabricated using the DOI or APE methods. For such cantilevers, the ion-damaged layer at the bottom of the cantilever primarily determines the total Q-factors. In this case, the strategy to achieve a high Q-factor is to deposit a thick diamond epilayer on top of the ion-implanted diamond substrate.52

As seen in Figure 3(a), the Q-factors for the diamond cantilevers fabricated by helium (He) ion implantation at 1 MeV were 2,000 ~ 7,000.31 Considering the composition of cantilevers with both an ion implantation damaged layer and a high quality homoepitaxial layer, a proposed bilayer model explains how the Q-factor varies with epilayer thickness, as follows53

| 1Q= 11+β (1Qepi + β1Qion) | (17) |
| --- | --- |

Here, Q represents the total Q-factor of the cantilever, Qepi is the Q-factor of the epilayer by itself, and Qion signifies the effective mechanical Q-factor of the ion-implantation damaged layer. The dimensionless factor β is defined as β=(Eiontion)/(Eepitepi), where Eion and Eepi stand for the ion-damaged layer’s and epilayer’s respective Young’s modulus. Additionally, tion and tepi represent the thickness of the ion-damaged layer and epilayer, respectively. The assumption Eion=Eepi simplifies β to tion/tepi. The decrease in β suggests a gradual elimination of the ion-damaged layer.

- Figure 3. (a) Q-factors as a function of cantilever length and width. (b) Q-factor dependence on the ion-damaged layer to epilayer thickness ratio. Reproduced with permission from reference 31. Copyright 2014 AIP Publishing. Reproduced with permission from reference 52. Copyright 2017 The Japan Society of Applied Physics.

As illustrated in Figure 3(b), the Qion of the cantilever with the ion-damaged layer alone exhibited a low Q-factor around 200.52 By growing a homoepitaxial layer with a thickness of 1.81 µm on ion-implanted SCD substrates, the Q-factor was significantly improved. It is clear from that with the increasing thickness ratio of the epilayer to the substrate, there is a corresponding increase in the Q-factor, this was found to be compatible with Equation (15).

## 3.2 Defects Engineering

(1) Reducing Defects

Evading or reducing energy dissipation caused by defects is crucial in attaining ultrahigh Q-factor resonators for applications in quantum platforms and high-sensitivity MEMS/NEMS sensors. The defects induced by ion-implantation have a detrimental impact on the Q-factors of diamond mechanical resonators. To improve the Q-factors, one effective strategy involves reducing the defects through annealing the as-fabricated diamond mechanical cantilevers in an ultrahigh vacuum (UHV) environment, as shown in Figure 4(a). We explored the effects of UHV annealing on the resonance properties of SCD cantilevers, and assessed the impact of ion-implantation damages in diamond by measuring the Q-factors of diamond resonators.45 After annealing the SCD cantilevers in the temperature range of 900°C to 1100°C and cleaning them with hydrogen plasma, as Figure 4(b) depicts, the resonance frequency and Q-factors were measured. As Figure 4(c) illustrating, the Q-factors significantly improved after annealing at 1100°C, rising from average values of approximately 8,000 to beyond 15,000. This method improved the Q-factor by reducing the effect of the defects in the ion-implanted diamond substrate.

- Figure 4. Digital photos of (a) UHV annealing and (b) H2 plasma treatment. (c) Q-factors of different cantilever length increase with increasing annealing temperatures and further H2 plasma cleaning. Reproduced with permission from reference 45. Copyright 2023 Elsevier B.V.

(2) Removing the Defective Layer

To boost the Q-factors of the SCD cantilevers, in addition to the growth of a thick high crystal-quality SCD layer, it is necessary to remove ion-implantation induced damaged layer at the bottom of the cantilever. We achieved ultra-high Q-factors over 1,000,000 in SCD resonators by the use of a smart-cut technique and atomic layer etching (ALE) with 1-nm accuracy.43 In the smart-cut technique, a high-energy ion beam (over 100 keV), was focused onto the SCD substrate, which caused a phase change in the diamond that would act as the sacrificial layer.54 Employing the ALE process in an oxygen ambient alongside high-quality diamond growth, we effectively removed the defective layer within SCD resonators with a thickness accuracy of less than 1 nm, consequently reducing the intrinsic energy dissipation in the cantilevers.

The thickness variation of the SCD cantilever was monitored by the resonance frequency shift. In our etching experiments conducted at 430°C and 500°C for varying durations, a noticeable resonance shift was observed after oxygen etching at 500°C for 4 h, as depicted in Figure 5(a).55 Figure 5(b) illustrates a marked improvement in Q-factors, increasing from 3,500 to 7,000 after annealing at 500°C for 7 h. The etching rate was estimated to be approximately 0.4 to 0.5 nm/h at a temperature of 500°C in an oxygen ambient, corresponding to a carbon mass loss of 10−12 g/h. As shown in Figure 5(c), the Q-factor of a 1.6 µm-thick diamond MEMS cantilever was markedly enhanced to 417,000 after annealing for 380 h in oxygen ambient at 500°C. For further investigation, the etching effect on resonance frequency and Q-factor at 500°C was examined, as displayed in Figure 5(d)-(e). Utilizing ring-down measurement techniques, the Q-factor surpassed 430,000 for a 1.44 µm thick and 100 µm long SCD cantilever, as shown in Figure 5(f). Following further oxygen etching and hydrogen plasma cleaning treatment resulted in the Q-factor eventually exceeding one million, higher than the values reported for PCD, NCD, monocrystalline silicon, and other crystalline materials.43 The diamond MEMS resonators thereby show great promise for sensor applications and coupling with quantum centers in diamond, with the key advancement being the ALE method providing nanometer thickness accuracy, enabling precise control over both the resonator’s quality and vertical dimension.

- Figure 5. (a) Resonance frequency shift after annealing at 500°C for 4 h in O2 atmosphere. (b) Dependence of Q-factor on the annealing time at 430°C and 500°C. (c) Ring-down curve after 380 h annealing in an O2 ambient. (d) Rsonance frequency shift after ALE treatment (500°C, 380 h). (e) Q-factor as a function of ALE durations. (f) Ring-down measurements before and after ALE for 380 h. Reproduced with permission from reference 55. Copyright 2017 Elsevier Ltd. Reproduced with permission from reference 43. Copyright 2018 American Physical Society.

## 3.3 Strain Engineering

Over the past fifteen years, dissipation dilution due to strain engineering has been demonstrated to increase in Q-factors by a four-order-of-magnitude, outperforming earlier the most advanced results in bulk crystalline resonators at both room temperature and liquid helium temperatures.28 The newly developed techniques of strain engineering have facilitated Q-factors of up to 3.6×109 at room temperature,56 while strained silicon resonators have achieved Q-factors of 1.3×1010 at 7 K.57

The combination of dissipation dilution through strain engineering with the high intrinsic Q-factors of single crystal materials may lead to extremely high Q-factors at room temperature. Given that SCD is an ideal single crystal material for MEMS/NEMS applications, it is imperative to explore the potential of strain engineering in SCD MEMS devices. To examine the impact of strain on the Q-factor of SCD, we fabricated double-clamped SCD NEMS resonators with different thickness. The resonance properties of the SCD bridges were further investigated. Figure 6 (a) displays the relationship between the resonance frequency (f) and length (L). The linearity of f vs L-2 length for the SCD NEMS beam deviated from the Euler-Bernoulli beam theory (Equation (3)) for long length. As shown in Fig. 6(b), the resonance frequency increases with thickness decreasing from 180 nm to 158 nm reduced by oxygen etching, which suggests the existence of tensile stress in the beam. In the meanwhile, as the thickness decreased from 180 nm to 166 nm, the Q-factor also increases due to the strain in the SCD NEMS beams. This experiment provides a promising approach to achieve exceptionally high Q-factors through the strategic utilization of strain engineering and thickness effects in SCD bridges.

- Figure 6. Resonance properties of double-clamped SCD NEMS beam with different thicknesses (a) Variation of resonance frequency with SCD bridge length. (b) Resonance frequency and Q-factor of a 100 μm long SCD bridge plotted against different thickness.

# 4. HIGH-ORDER RESONANCE TOWARD HIGH f‧Q PRODUCTS

When sensing relies on frequency shift, the Q-factor becomes crucial. However, higher resonance frequency typically results in a reduction in the Q-factor for the first-order resonance because of the heightened dissipation. The product of resonance frequency (f) and Q-factor f‧Q emerges as a key parameter for MEMS/NEMS devices. In order to obtain increased sensitivity, quick response times, and better tolerance to mechanical noise, a high f‧Q value is desired. It has been demonstrated that high-order resonance modes can improve sensing capabilities, including the mass sensitivity of a cantilever and the scanning speed and image contrast of AFM.

- Figure 7. Variation of Q-factor and f∙Q shift with (a) lengths and (b) resonance orders for diamond cantilevers. (c) Resonance frequency spectra and (d) ring-down measurement on a diamond cantilever at its second resonance mode. Reproduced with permission from reference 14. Copyright 2024 The Authors.

As we examine the resonance characteristics and energy dissipation in the initial three resonance modes, the f‧Q product increases significantly at higher orders, as Figure 7(a) shows.14 Figure 7(b) illustrates the roughly 15-time rise in the f‧Q product at the third-order resonance, with the Q-factor remaining almost unchanged. Higher order resonances have less clamping loss compared to the fundamental mode, possibly because nodes further away from the clamping points store more mechanical energy. As can be seen in Figure 7(c)-(d), we achieved an ultra-high f‧Q product above 1012 Hz through higher-order resonances in the diamond cantilevers. The improvement in f‧Q was attained without the requirement for extra treatments, like UHV annealing or surface etching. This work offers promising applications for diamond mechanical cantilevers, including the field of AFM tips, mass, and magnetic sensors.

# 5. CONCLUDING REMARKS

In this Account, the strategies for improving the Q-factor of diamond MEMS/NEMS by reducing the energy dissipations with the resonators are reviewed, mainly drawing insights from our group’s research to date. The combination of overgrowth of high-crystal quality diamond epilayers and reactive etching represent the primary methods employed to enhance the Q-factor of diamond mechanical resonators fabricated through the smart-cut technique. Removing the defective layer caused by ion irradiation at the bottom of the SCD MEMS beams resulted in a remarkable increase in the Q-factor from around 10,000 to over a million. The intrinsic Q-factor of SCD MEMS resonators exceeds those of other semiconductor materials at room temperature. The further enhancement of the Q-factors of SCD MEMS/NEMS at room temperature may be achieved through the dissipation dilution via strain engineering. The fabrication of SCD bridge structures with nanoscale dimensions is well-suited for enhancing Q-factors through strain engineering. By optimizing sample geometry and refining nanofabrication processes, deep elastic strain engineering—inducing high (>5%) tensile or shear elastic strains in diamond—has the potential to significantly improve Q-factors. The Q-factor and its enhancement techniques constitute paramount features for diamond MEMS/NEMS applications, given that a higher Q-factor contributes to higher sensitivity, resolution, and higher reliability. Research on improving Q-factors of diamond MEMS/NEMS paves the way for the advancement of next-generation integrated MEMS/NEMS and optomechanical systems, significantly boosting the performance and reliability for ultra-sensitive sensors and quantum sciences.

The merits of diamond MEMS for high-reliability sensors were revealed. All electrical-type on-chip SCD MEMS resonators were demonstrated and parallel readout of resonator arrays was achieved. The SCD MEMS magnetic sensors showed high reliability up to 500oC. The utilization of high-Q factors SCD NEMS resonators would improve the magnetic sensitivity toward pico-Tesla. Nevertheless, the interface energy dissipation between the functional magnetic materials with SCD NEMS requires further deep investigation. The being increased size of SCD wafers would push forward the development of diamond MEMS/NEMS for wide applications in physical, chemical, medical, and biological fields, where point defects are less critical compared to electronic devices. Further advances in diamond MEMS/NEMS integrating with complementary metal-semiconductor-oxide (CMOS) circuits should be explored to achieve practical applications that conventional MEMS devices cannot reach.

- AUTHOR INFORMATION

Corresponding Author

Meiyong Liao - Research Center for Electronic and Optical Materials, National Institute for Materials Science, Tsukuba, Ibaraki 305-0044, Japan; orcid.org/0000-0003-1361-4266; Email: Meiyong.Liao@nims.go.jp

Authors

Guo Chen - School of Materials Science and Technology, China University of Geosciences, Beijing 100083, China; Research Center for Electronic and Optical Materials, National Institute for Materials Science, Tsukuba, Ibaraki 305-0044, Japan

Satoshi Koizumi - Research Center for Electronic and Optical Materials, National Institute for Materials Science, Tsukuba, Ibaraki 305-0044, Japan

Yasuo Koide - Research Center for Electronic and Optical Materials, National Institute for Materials Science, Tsukuba, Ibaraki 305-0044, Japan

Biographies

Guo Chen earned his Bachelor’s degree and became a Master student in material science and technology at China University of Geosciences (Beijing) in 2018. He is now pursuing a Ph.D. in material science and technology at China University of Geosciences (Beijing) since 2019. He is also a visiting Ph.D. student at National Institute for Materials Science (NIMS) in Japan since 2022. His current research mainly focuses on single-crystal diamond micro-electromechanical systems (MEMS) resonators for developing high-performance sensors, and the basic material science in the field of ultra-wide bandgap semiconductors, and flexible composite phase change materials (PCMs) for energy storage.

Satoshi Koizumi received a Ph.D. degree in Electrical and Electronic Engineering from Aoyama Gakuin University in 1993. He is now the group leader of the ultra-wide bandgap semiconductors group at National Institute for Materials Science (NIMS). He has worked on functional materials, devices and electronic equipment.

Yasuo Koide received a Ph.D. degree in Electronic Engineering from Nagoya University in 1988. He is now the group leader of the next-generation semiconductor group at National Institute for Materials Science (NIMS). He has worked on semiconductor materials and devices.

Meiyong Liao obtained B.S. (1996) and M.S. degrees (1999) from Lanzhou University, China and Ph.D. degree (2002) from Institute of Semiconductors, Chinese Academy of Sciences (joint with COSDAF, City University of Hong Kong). He was a visiting associate professor at Kyoto University from 2002 to 2004. In 2004, he joined National Institute for Materials Science (NIMS), Japan, as a postdoctor researcher and was then employed as a senior researcher in 2008. He is now a chief researcher at NIMS, Japan. His current research interests cover diamond growth, MEMS, and semiconductor electronic and photonic devices.

- ACKNOWLEDGEMENTS

This work was supported by JSPS KAKENHI (Grant Number 22K18957, 24H00287), Bilateral joint research between JSPS/CAS, ARIM of MEXT (JPMXP1223NM5297). Guo Chen thanked to financial support from China Scholarship Council (No. 202006400023).

- REFERENCES

- Sun, H.; Zhang, Z.; Liu, Y.; Chen, G.; Li, T.; Liao, M. Diamond MEMS: From Classical to Quantum. Adv. Quantum. Technol. 2023, 6 (11), 2300189.

- Henry Huang, X. M.; Zorman, C. A.; Mehregany, M.; Roukes, M. L. Nanodevice motion at microwave frequencies. Nature 2003, 421 (6922), 496-496.

- Imboden, M.; Mohanty, P. Dissipation in nanoelectromechanical systems. Phys. Rep. 2014, 534 (3), 89-146.

- Liao, M. Progress in semiconductor diamond photodetectors and MEMS sensors. Functional Diamond 2022, 1 (1), 29-46.

- Yang, N.; Foord, J. S.; Jiang, X. Diamond electrochemistry at the nanoscale: A review. Carbon 2016, 99, 90-110. DOI: https://doi.org/10.1016/j.carbon.2015.11.061.

- Nebel, C. E. CVD diamond: a review on options and reality. Functional Diamond 2023, 3 (1), 2201592. DOI: 10.1080/26941112.2023.2201592.

- Sumant, A. V.; Auciello, O.; Liao, M.; Williams, O. A. MEMS/NEMS based on mono-, nano-, and ultrananocrystalline diamond films. Mrs. Bull. 2014, 39 (6), 511-516.

- Leigh, W. G. S.; Cuenca, J. A.; Thomas, E. L. H.; Mandal, S.; Williams, O. A. Mapping the effect of substrate temperature inhomogeneity during microwave plasma-enhanced chemical vapour deposition nanocrystalline diamond growth. Carbon 2023, 201, 328-337.

- Yamamoto, A.; Nawachi, N.; Tsutsumoto, T.; Terayama, A. Pressure sensor using p-type polycrystalline diamond piezoresistors. Diam. Relat. Mater. 2005, 14 (3-7), 657-660.

- Auciello, O.; Aslam, D. M. Review on advances in microcrystalline, nanocrystalline and ultrananocrystalline diamond films-based micro/nano-electromechanical systems technologies. J. Mate.R Sci. 2021, 56 (12), 7171-7230.

- Zhang, Z.; Zhao, W.; Chen, G.; Toda, M.; Koizumi, S.; Koide, Y.; Liao, M. On-chip Diamond MEMS Magnetic Sensing through Multifunctionalized Magnetostrictive Thin Film. Adv. Funct. Mater. 2023, 33 (27), 2300805. DOI: https://doi.org/10.1002/adfm.202300805.

- Fu, J.; Zhu, T.; Liang, Y.; Liu, Z.; Wang, R.; Zhang, X.; Wang, H.-X. Fabrication of capacitive pressure sensor using single crystal diamond cantilever beam. Sci. Rep. 2019, 9 (1), 4699.

- Liao, M.; Hishita, S.; Watanabe, E.; Koizumi, S.; Koide, Y. Suspended single‐crystal diamond nanowires for high‐performance nanoelectromechanical switches. Adv. Mater. 2010, 22 (47), 5393-5397.

- Chen, G.; Zhang, Z.; Gu, K.; Sang, L.; Koizumi, S.; Toda, M.; Ye, H.; Koide, Y.; Huang, Z.; Liao, M. Higher-order resonance of single-crystal diamond cantilever sensors toward high f‧ Q products. Appl. Phys. Express. 2024, 17 (2), 021001.

- Koide, Y.; Liu, J.; Liao, M.; Imura, M. Diamond FET and MEMS Dvivices. In 2023 IEEE International Symposium on Applications of Ferroelectrics (ISAF), 2023; IEEE: pp 1-4.

- Burek, M. J.; De Leon, N. P.; Shields, B. J.; Hausmann, B. J.; Chu, Y.; Quan, Q.; Zibrov, A. S.; Park, H.; Lukin, M. D.; Lončar, M. Free-standing mechanical and photonic nanostructures in single-crystal diamond. Nano. Lett. 2012, 12 (12), 6084-6089.

- Burek, M. J.; Ramos, D.; Patel, P.; Frank, I. W.; Lončar, M. Nanomechanical resonant structures in single-crystal diamond. Appl. Phys. Lett. 2013, 103 (13), 131904.

- Tao, Y.; Degen, C. Facile Fabrication of Single-Crystal-Diamond Nanostructures with Ultrahigh Aspect Ratio. Adv. Mater. 2013, 25 (29), 3962-3967.

- Tao, Y.; Boss, J. M.; Moores, B.; Degen, C. L. Single-crystal diamond nanomechanical resonators with quality factors exceeding one million. Nat. Commun. 2014, 5 (1), 3638.

- Ovartchaiyapong, P.; Pascal, L.; Myers, B.; Lauria, P.; Bleszynski Jayich, A. High quality factor single-crystal diamond mechanical resonators. Appl. Phys. Lett. 2012, 101 (16), 163505.

- Liao, M.; Koide, Y. Carbon-based materials: growth, properties, MEMS/NEMS technologies, and MEM/NEM switches. Crit. Rev. Solid. State. 2011, 36 (2), 66-101.

- Zhang, Z.; Wu, Y.; Sang, L.; Wu, H.; Huang, J.; Wang, L.; Takahashi, Y.; Li, R.; Koizumi, S.; Toda, M.; Akita, I. M.; Koide Y; Liao, M. Coupling of magneto-strictive FeGa film with single-crystal diamond MEMS resonator for high-reliability magnetic sensing at high temperatures. Mater. Res. Lett. 2020, 8 (5), 180-186.

- Zhang, Z.; Sang, L.; Wu, H.; Huang, J.; Wang, L.; Koizumi, S.; Kodie, Y.; Liao, M. Galfenol-Ti-Diamond multilayer MEMS resonator for magnetic sensor working up to 773 K. In 2019 IEEE International Electron Devices Meeting (IEDM), 2019; IEEE: pp 34.6.1-34.6.4.

- Shen, X.; Sun, H.; Sang, L.; Imura, M.; Koide, Y.; Koizumi, S.; Liao, M. Integrated TbDyFe Film on a Single‐Crystal Diamond Microelectromechanical Resonator for Magnetic Sensing. Phys Status Solidi-R. 2021, 15 (9), 2100352.

- Liao, M.; Sang, L.; Sun, H.; Li, T.; Koizumi, S. Highly efficient diamond electromechanical transducer based on released metal–oxide–semiconductor structure. Appl. Phys. Lett. 2021, 119 (7), 1-5.

- Voiculescu, I.; Liao, M.; Zakerin, M.; Berger, R.; Ono, T.; Toda, M. Pico-thermogravimetric material properties analysis using diamond cantilever beam. Sensor. Actuat. A-Phys. 2018, 271, 356-363.

- Sun, H.; Shen, X.; Sang, L.; Imura, M.; Koide, Y.; You, J.; Li, T.-F.; Koizumi, S.; Liao, M. Thermal mismatch induced stress characterization by dynamic resonance based on diamond MEMS. Appl. Phys. Express. 2021, 14 (4), 045501.

- Engelsen, N. J.; Beccari, A.; Kippenberg, T. J. Ultrahigh-quality-factor micro-and nanomechanical resonators using dissipation dilution. Nat. Nanotechnol. 2024, 19, 1-13, DOI: https://doi.org/10.1038/s41565-023-01597-8.

- Yasumura, K. Y.; Stowe, T. D.; Chow, E. M.; Pfafman, T.; Kenny, T. W.; Stipe, B. C.; Rugar, D. Quality factors in micron-and submicron-thick cantilevers. J. Microelectromech. S. 2000, 9 (1), 117-125.

- Heinrich, S. M.; Dufour, I. Fundamental theory of resonant MEMS devices. In Resonant MEMS: Fundamentals, Implementation and Application; Brand O, Dufour I, Heinrich S, Josse F, Fedder G, Hierold C, Korvink J, Tabata O; Chapter 1; 2015, 1-28.

- Liao, M.; Toda, M.; Sang, L.; Hishita, S.; Tanaka, S.; Koide, Y. Energy dissipation in micron-and submicron-thick single crystal diamond mechanical resonators. Appl. Phys. Lett. 2014, 105 (25), 251904.

- Imboden, M. Diamond nanoelectromechanical resonators: Dissipation and superconductivity; Boston University, 2012.

- Schmid, S.; Hierold, C. Damping mechanisms of single-clamped and prestressed double-clamped resonant polymer microbeams. J. Appl. Phys. 2008, 104 (9), 093516.

- Chen, Y.; Sang, L.; Koizumi, S.; Koide, Y.; Liu, X.; Liao, M. Effect of gas pressure on the quality-factor of single-crystal diamond micro cantilevers. Diam. Relat. Mater. 2022, 129, 109340.

- Jimbo, Y.; Itao, K. Energy loss of a cantilever vibrator. J Horological Institute of Japan 1968, 47, 1-15.

- Imboden, M.; Mohanty, P.; Gaidarzhy, A.; Rankin, J.; Sheldon, B. W. Scaling of dissipation in megahertz-range micromechanical diamond oscillators. Applied Physics Letters 2007, 90 (17), 173502.

- Photiadis, D. M.; Judge, J. A. Attachment losses of high Q oscillators. Appl. Phys. Lett. 2004, 85 (3), 482-484.

- Lifshitz, R.; Roukes, M. L. Thermoelastic damping in micro-and nanomechanical systems. Phys. Rev. B. 2000, 61 (8), 5600.

- Sun, H.; Sang, L.; Wu, H.; Zhang, Z.; Teraji, T.; Li, T.-F.; You, J.; Toda, M.; Koizumi, S.; Liao, M. Effect of deep-defects excitation on mechanical energy dissipation of single-crystal diamond. Phys. Rev. Lett. 2020, 125 (20), 206802.

- Wachtman Jr, J.; Tefft, W.; Lam Jr, D.; Apstein, C. Exponential temperature dependence of Young's modulus for several oxides. Physical Review 1961, 122 (6), 1754.

- Yang, J.; Ono, T.; Esashi, M. Energy dissipation in submicrometer thick single-crystal silicon cantilevers. J. Microelectromech. S. 2002, 11 (6), 775-783.

- Liao, M.; Koide, Y.; Sang, L. Single crystal diamond micromechanical and nanomechanical resonators. In Novel Aspects of Diamond: From Growth to Applications; Yang, N; Vo1.21; Chapter 4; 2019, 91-121.

- Wu, H.; Sang, L.; Li, Y.; Teraji, T.; Li, T.; Imura, M.; You, J.; Koide, Y.; Toda, M.; Liao, M. Reducing intrinsic energy dissipation in diamond-on-diamond mechanical resonators toward one million quality factor. Phys. Rev. Mater. 2018, 2 (9), 090601.

- Shen, X.; Lv, Z.; Ichikawa, K.; Sun, H.; Sang, L.; Huang, Z.; Koide, Y.; Koizumi, S.; Liao, M. Stress effect on the resonance properties of single-crystal diamond cantilever resonators for microscopy applications. Ultramicroscopy 2022, 234, 113464.

- Chen, G.; Zhang, Z.; Koide, Y.; Koizumi, S.; Huang, Z.; Liao, M. Disclosing the annihilation effect of ion-implantation induced defects in single-crystal diamond by resonant MEMS. Diam. Relat. Mater. 2023, 138, 110240.

- Zhang, Z.; Chen, G.; Gu, K.; Koizumi, S.; Liao, M. Effect of defects on Q factors of single-crystal diamond MEMS resonators. Functional Diamond 2023, 3 (1), 2221280.

- Gaidarzhy, A.; Imboden, M.; Mohanty, P.; Rankin, J.; Sheldon, B. W. High quality factor gigahertz frequencies in nanomechanical diamond resonators. Appl. Phys. Lett. 2007, 91 (20), 203503.

- Adiga, V. P.; Sumant, A.; Suresh, S.; Gudeman, C.; Auciello, O.; Carlisle, J.; Carpick, R. W. Mechanical stiffness and dissipation in ultrananocrystalline diamond microresonators. Phys. Rev. B. 2009, 79 (24), 245403.

- Poggio, M.; Jura, M.P.; Degen, C.L.; Topinka, M.A.; Mamin, H.J.; Goldhaber-Gordon, D; Rugar, D. An off-board quantum point contact as a sensitive detector of cantilever motion. Nat. Phys. 2008, 4(8), 635-638.

- Gigan, S.; Böhm, H.R.; Paternostro, M.; Blaser, F.; Langer, G.; Hertzberg, J.B.; Schwab, K.C.; Bäuerle, D.; Aspelmeyer, M.; Zeilinger, A. Self-cooling of a micromirror by radiation pressure. Nature 2006, 444(7115), 67-70.

- Anetsberger, G.; Arcizet, O.; Unterreithmeier, Q.P.; Rivière, R.; Schliesser, A.; Weig, E.M.; Kotthaus, J.P; Kippenberg, T.J.; Near-field cavity optomechanics with nanomechanical oscillators. Nat. Phys. 2009, 5(12), 909-914.

- Liao, M.; Toda, M.; Sang, L.; Teraji, T.; Imura, M.; Koide, Y. Improvement of the quality factor of single crystal diamond mechanical resonators. Jpn. J. Appl. Phys. 2017, 56 (2), 024101.

- Seitner, M. J.; Gajo, K.; Weig, E. M. Damping of metallized bilayer nanomechanical resonators at room temperature. Appl. Phys. Lett. 2014, 105 (21), 213101.

- Parikh, N.; Hunn, J.; McGucken, E.; Swanson, M.; White, C.; Rudder, R.; Malta, D.; Posthill, J.; Markunas, R. Single‐crystal diamond plate liftoff achieved by ion implantation and subsequent annealing. Appl. Phys. Lett. 1992, 61 (26), 3124-3126.

- Wu, H.; Sang, L.; Teraji, T.; Li, T.; Wu, K.; Imura, M.; You, J.; Koide, Y.; Liao, M. Reducing energy dissipation and surface effect of diamond nanoelectromechanical resonators by annealing in oxygen ambient. Carbon 2017, 124, 281-287.

- Bereyhi, M. J.; Arabmoheghi, A.; Beccari, A.; Fedorov, S. A.; Huang, G.; Kippenberg, T. J.; Engelsen, N. J. Perimeter modes of nanomechanical resonators exhibit quality factors exceeding 10 9 at room temperature. Phys. Rev. X. 2022, 12 (2), 021036.

- Beccari, A.; Visani, D. A.; Fedorov, S. A.; Bereyhi, M. J.; Boureau, V.; Engelsen, N. J.; Kippenberg, T. J. Strained crystalline nanomechanical resonators with quality factors above 10 billion. Nat. Phys. 2022, 18 (4), 436-441.

- TOC/Abstract graphic

- For Table of Contents Only

- Title: "Low-energy Dissipation Diamond MEMS"

Authors: Chen, Guo; Koizumi, Satoshi; Koide, Yasuo; Liao, Meiyong