## Slide 1
Biomimetic Hot-Melt Adhesive Using Galloyl-Grafted Polypropylene for Multisubstrates
Paripat Kraisornkachit, PhD
Research Center for Macromolecules and Biomaterials
National Institute for Materials Science (NIMS), Japan
ACS Appl. Polym. Mater. 2026 DOI: https://doi.org/10.1021/acsapm.6c01626

## Slide 2
Adhesive Materials
Thermoplastic Adhesives
Thermosetting Adhesives
Automotive
Electronics
Packaging
Substrate
Adhesive layer
Lightweight
Design flexibility
Thermal management
Fast processing
Thermosetting adhesives offer high adhesive performance, but their long bonding time needs an improvement.
Thermoplastic adhesives enable simple bonding, yet their adhesive performance remains challenging.
Substrate
Substrate
Substrate
Substrate
Adhesive layer
[1] Characteristics of Adhesive Materials. In Adhesives Technology Handbook; Elsevier, 2009; pp 63–135. [2] Chung, S. W. et al. Microelectronics Reliability 2012, 52 (7), 1501–1510.

## Slide 3
[3] Chen, M.-A. et al. International Journal of Adhesion & Adhesives 2007, 27, 175–187.
Maleic anhydride grafted polypropylene (PPMA) is one of the commercially available Hot-Melt Adhesive (HMA).
Resin
Hardener
Fast Bonding
No Mixing Required
Reheated Ability
Adhesive Joint
Strength (MPa)
Epoxy
Adhesive
HMA[3]
10
−
−
−
20
30
Major Limitation of HMA is a significantly lower adhesive strength compared to epoxy-based systems.
Maleic anhydride
Epoxy-based adhesive
Hot-melt adhesive
Low Cost
Improving adhesive strength of HMA while reducing bonding time is challenging for adhesive material development.
Long Bonding Time
Thermosetting polymer
Epoxy
Curing agent
Adhesive Joint
Strength (MPa)
Epoxy
Adhesive
HMA[3]
10
−
−
−
20
30
Improving adhesive strength of HMA is challenging

## Slide 4
Maleic Anhydride Grafted Polypropylene[4]
Hydrogen
abstraction
β-scission
Simple grafting process using only heat and peroxide initiator
β-scission (side reaction) severely degrades the polymer causing poor mechanical properties
Adhesion Mechanism[5]
[4] Zhang, M. et al. Macromolecules 2013, 46, 4313−4323. [5] Chen, M-A. et al. International Journal of Adhesion & Adhesives 2007, 27, 175–187.
Hydroxyl groups formed via the hydrolysis of maleic anhydride interact with the hydroxylated metal surface to drive interfacial bonding.

## Slide 5
Catechol Group
[6] Lyu, Q. et al. ACS Biomater. Sci. Eng. 2019, 5, 6, 2708–2724. [7] Panchireddy, S. et al. ACS Sustainable Chem. Eng. 2018, 6, 14936−14944.
[8] Zhan, K. et al. Biomacromolecules 2017, 18, 2959−2966.
Catechol Containing Polyhydroxyurethanes[7]
Catechol moiety can interact with different inorganic or organic surfaces[6]
Galloyl Group[8]
P(VGal-co-BA)
P(VCat-co-BA)
P(VSt-co-BA)
P(VPh-co-BA)
Gallic acid
Galloyl functionalized polymer with much more hydroxyl group achieved stronger adhesion performance

## Slide 6
[9] Payra, D. et al. Polym. Chem., 2017, 8, 1654–1663. [10] Fujita, T. et al. Materials 2023, 16, 266.
Previous Studies from our Group
Biomimetic Catechol-Functionalized[9]
Galloyl-Functionalized[10]
X = H
Hydroxyl (-OH) group plays a crucial role in the adhesion of polymers to various substrates through hydrogen bonding, polarity improvements, and chemical reactivity.
A biomimetic adhesive design by functionalized catechol as pendant functional moieties for surface anchoring. However, the maximum lap shear strength remains low (~6 MPa).
Remarkable adhesive strength (10 MPa) recently obtained via a simple and inexpensive preparation method.
Grafting galloyl functional group onto polypropylene for adhesive applications has not been previously reported.

## Slide 7
Gallic-acid-bearing methacrylate (GAMA)
Benzoyl methacrylate (BAMA)
3,4-dihydroxyphenethyl methacrylate (DHPM)
Maleic anhydride (MAH)
Sample name | Grafting reagent | Grafting reagent ratio (mol %) | Incorporation amount (mol %)
Pristine PP | − | 0 | 0
PPGA6.2 | GAMA | 15.9 | 6.2
PPGA8.9 | GAMA | 27.5 | 8.9
PPGA10.6 | GAMA | 36.2 | 10.6
PPGA11.8 | GAMA | 43.1 | 11.8
PPBA | BAMA | 27.5 | 2.8
PPCA | DHPM | 27.5 | 0.9
PPMA | MAH | 27.5 | 8.0
PPGA
PPBA
PPCA
PPMA
Materials and Reaction Schemes
Simple grafting by using peroxide initiator

## Slide 8
Preparation of Adhesive Films and Lap Shear Specimens
Polymer pallets
Teflon
spacer
Grafting with solvent method
Purification with Methanol
Drying
Adhesive film preparation
175 °C 10 MPa 5 min
Lap shear specimen preparation
160 °C / 175 °C 0.5 MPa 3 min
Adhesive film
Metal or PP substrates
Substrate
Substrate
Load
Lap shear tests
Hot-melt adhesives requiring 3 minutes of hot pressing under low pressure enable a fast-bonding process
Grafting with reactive extrusion (REX)
Industrial Applicability

## Slide 9
Adhesives
Unmodified PP
Grafted PP
Pristine PP
PPGA
PPBA
PPCA
PPMA
PPGA → 15.9, 27.5, 36.2 and 43.1 mol%
PPBA, PPCA and PPMA → 27.5 mol%
Adhesive Testing
Substrate
Substrate
Load
Adhesive Characterization
Charazterization | Instrument
Incorporation of functional group | FTIR
Incorporation amount | Elemental analysis
Thermal properties | DSC
Crystallinity | DSC, XRD
Interfacial analysis | STEM, XPS
Fracture behavior | Image camera
Substrates | 
Dry adhesion | Wet adhesion
PP | PP
Aluminum | 
Stainless steel | 
Copper | 

## Slide 10
Incorporation of Functional Group
Instrument: FTIR
O–H
stretching
CH3 and CH2 stretching
C=O stretching
Normalized CH3 stretching
C=O stretching
FTIR peaks at 3496 cm⁻¹ (O–H) and 1716 cm⁻¹ (C=O) confirm successful galloyl functionalization of PPGA.[11]
Normalized spectra exhibit a rise in the C=O peak with higher GAMA content, indicating increased grafting of the galloyl functional group.
[11] Hirun, N. et al. Spectrochim. Acta. A Mol. Biomol. Spectrosc. 2012, 86, 93–100.
PPGA

## Slide 11
Instrument: FTIR
PPBA
PPMA
PPCA
FTIR peak at 1716 cm⁻¹ (C=O stretching) confirm successful Benzoyl functionalization of PPBA.
Cyclic anhydride stretching peaks at 1780 and 1850 cm⁻¹ confirm successful maleic anhydride functionalization of PPBA.
It is noteworthy that PPCA shows only a weak carbonyl (C=O) stretching peak at 1700 cm⁻¹.
Incorporation of Functional Group

## Slide 12
Thermal Properties
Instrument: DSC
PPGA and PPCA samples exhibit slightly higher melting temperatures (Tm) than pristine PP, while PPBA and PPMA show slightly lower Tm.
The increase in Tm​ may be attributed to enhanced intermolecular interaction of the functional groups.

## Slide 13
Crystallinity
Instrument: DSC and XRD
Crystallinity of PPGAs decreases by ~20–40%, yet Tm increases—likely due to hydrogen bonding, π–π stacking, and CH–π interactions among galloyl groups in the amorphous phase.
XRD confirms reduced crystallinity with increasing galloyl content, shown by:
- Lower intensity of α-phase reflections (α(110), α(040), α(130), α(111))
- Slight shifts to lower 2θ, indicating disrupted chain packing and increased amorphous fraction.

## Slide 14
Mechanical Properties of PPGA Films
Increasing the galloyl functionalization led to a deterioration of mechanical performance, resulting in a more brittle characteristic in the PPGA adhesive films.
Beyond an incorporation amount of 8.9 mol%, the PPGA films became increasingly brittle; this loss of ductility led to a subsequent reduction in lap shear performance.

## Slide 15
Sample name | Preparation ratio (mol %) | Incorporation ratioa (mol %) | Mwb × 103 (g⋅mol-1) | Ðb | Tmc (°C) | Xcc (%)
Pristine PPd | 0 | 0 | 308.4 | 4.4 | 161.6 | 52.7
PPGA6.2 | 15.9 | 6.2 | 331.7 | 3.7 | 165.7 | 32.5
PPGA8.9 | 27.5 | 8.9 | 321.0 | 3.1 | 165.7 | 23.9
PPGA10.6 | 36.2 | 10.6 | 350.0 | 3.9 | 165.8 | 17.1
PPGA11.8 | 43.1 | 11.8 | 344.5 | 4.4 | 167.4 | 10.0
PPBA | 27.5 | 2.8 | 262.3 | 3.5 | 157.2 | 41.4
PPMA | 27.5 | 8.0 | 94.0 | 2.6 | 154.0 | 37.9
PPCA | 27.5 | 0.9 | 389.2 | 4.9 | 163.9 | 39.0
Summary of Characterization of Pristine PP / Grafted PPs
PPGA retains a higher molecular weight compared to other functionalized PPs, indicating fewer degradative side reactions during grafting (suppression of β-scission)

## Slide 16
Adhesive Performance on PP Substrate
Testing: Single lap shear
PPGA8.9 and PPGA10.6 showed the highest lap shear strength on PP substrates, outperforming all other adhesives, as evidenced by necking and whitening of the PP substrate (substrate failure).
PPCA (with catechol group) exhibited no adhesion because catechol groups oxidized to quinones during synthesis.
100x playback speed

## Slide 17
Interfacial Analysis
Instrument: STEM
Clear interfacial layers were observed between PP substrate and PPGA adhesives, indicating effective interdiffusion and partial fusion during hot pressing.
PPGA6.2 exhibited a dense, continuous lamellar structure extending from PP substrate into the adhesive, while PPGA10.6 showed a broader amorphous interphase with fewer lamellae.
This amorphous layer accommodates mechanical deformation and stress distribution across the joint contributing to higher toughness and resistance to interfacial failure.[12]
[12] Yui, N. et al. Polym. J. 1995, 27, 614–622.

## Slide 18
Adhesive Performance on Metal Substrates
Testing: Single lap shear
PPGA8.9 demonstrated superior lap shear performance on aluminum stainless steel and copper substrates, outperform the commercially available and previously reported HMAs.
The PPGA adhesive still exhibited satisfactory adhesion strength after repeated use, emphasizing the reuseable benefit of hot-melt adhesive.
Reuseable performance on stainless steel substrate
[13] Kruszynski, J. et al. ACS Appl. Polym. Mater. 2023, 5 (5), 3875–3882. [14] Payra, D. et al. Polym. Chem. 2017, 8 (10), 1654–1663. [15] Evans, A. et al. ACS Appl. Mater. Interfaces 2025, 17 (23), 34592–34601.

## Slide 19
Industrial Applicability
PPGA6.2 adhesive prepared by reactive extrusion (REX), exhibited a remarkable lap-shear strength of 16.7 MPa on SS substrate, highlighting the industrial applicability of the proposed PPGA adhesive.
PP, gallic acid, and a peroxide initiator were simultaneously fed into the REX with twin-screw extruder at 190 °C. The grafting process was completed in only 8 minutes, resulting in improved processability.
Feed hopper
Controller
Twin-screw extruder
Heating chamber
Reactive extrusion (REX)

## Slide 20
Stability Performance
Environmental Aging Test for 7 Days
Test standard : JIS K7350-2-10 (BST) Cycle : Irradiation 102 min
Irradiation and water spay 18 min (total 120min) Irradiance broadband (300 – 400 nm) : 60 ± 2 W/m2 Irradiance narrowband (340 nm) : 0.51 ± 0.02 W/(m2 •nm) Black panel Temperature : 63 ± 3 °C Relative humidity : 50 ± 10 %
Total 50 times

## Slide 21
Stability Performance
Wet Adhesion
Environmental Aging Test for 7 Days
PPGA8.9 was able to maintain the excellent wet adhesion performance on stainless steel substrates even after immersion under water at 60 °C for 7 days
According to the environmental test standard (JIS K7350-2-10), PPGA8.9 maintained satisfactory adhesion performance under severe aging conditions, retaining 57% of its original

## Slide 22
Summary
Successfully grafting galloyl functional groups onto polypropylene (PPGA) via a straightforward, scalable process allows traditional hot-melt adhesives to achieve epoxy-like adhesion while maintaining the rapid-bonding advantages of thermoplastics—bridging the gap between processing speed and structural performance
The incorporation of galloyl groups onto polypropylene (PPGA) reduces crystallinity and increases the amorphous phase; this structural change, combined with the presence of hydroxyl groups, plays a crucial role in achieving excellent adhesion strength
PPGA adhesives exhibit excellent stability even under severe testing conditions, including wet adhesion and accelerated environmental aging

## Slide 23
Acknowledgement
This work was supported by the New Energy and Industrial Technology Development Organization (NEDO). The author expresses sincere gratitude to Prof. Masanobu Naito (NIMS), Prof. Yasuyuki Nakamura (NIMS), Mr. Kiyotaka Hitomi (NIMS), Ms. Mika Mano (NIMS), Prof. Shin Horiuchi (AIST) and Prof. Chiaki Sato (Institute of Science Tokyo) for their invaluable guidance and support throughout this project.