Controllable Andreev Bound States in Bilayer Graphene Josephson Junctions from Short to Long Junction Limits

Geon-Hyoung Park1, Wonjun Lee1,2, Sein Park1, Kenji Watanabe3, Takashi Taniguchi4,

Gil Young Cho1,2,5 and Gil-Ho Lee1,5*

1Deparment of Physics, Pohang University of Science and Technology, Pohang, Republic of Korea

2Center for Artificial Low Dimensional Electronic Systems, Institute for Basic Science, Pohang, Republic of Korea

3Research Center for Electronic and Optical Materials, National Institute for Materials Science, 1-1 Namiki, Tsukuba 305-0044, Japan

4Research Center for Materials Nanoarchitectonics, National Institute for Materials Science, 1-1 Namiki, Tsukuba 305-0044, Japan

5Asia Pacific Center for Theoretical Physics, Pohang, Republic of Korea

Abstract

We demonstrate that the mode number of Andreev bound states in bilayer graphene Josephson junctions can be modulated by controlling the superconducting coherence length in situ. By exploiting the quadratic band dispersion of bilayer graphene, we control the Fermi velocity and thus the coherence length via the application of electrostatic gating. Tunneling spectroscopy of the Andreev bound states reveals a crossover from short to long Josephson junction regimes as we approach the charge neutral point of the bilayer graphene. Furthermore, analysis of different mode numbers of the Andreev energy spectrum allows us to estimate the phase-dependent Josephson current quantitatively. Our work provides a new way for studying multi-mode Andreev levels by tuning the Fermi velocity.

In a superconductor–normal material–superconductor (SNS) Josephson junction (JJ), Cooper pairs can be transferred from one superconductor to another via the normal channel as coherently coupled electron–hole pairs generated by consecutive Andreev reflections at the SN interfaces [1-3]. Standing waves of Andreev pairs in the normal channel form Andreev bound states (ABS), which play a key role in governing the physics of SNS junctions. Recently, there has been growing interest in ABS in topological superconductivity research [4-6], quantum information processing [7-9], quantum states manipulation [10-12], and characterizing the topology of the Fermi sea [13,14].

ABS come in pairs at positive and negative energies due to the particle–hole symmetry of the superconductivity, and their energies oscillate periodically with the macroscopic superconducting phase difference between the two superconductors of the JJ. The number of ABS is determined by the ratio between the superconducting coherence length (ξ0) and channel length (L). For a ballistic conductor, the superconducting coherence length is given by the Fermi velocity νF and the superconducting gap Δ as ξ0=ℏvF/2Δ, and it determines the short (L≪ξ0) or long (L≫ξ0) junction limit [3,15]. Conventionally, short junctions have one ABS pair and long junctions have two or more. ABS in short junctions have been observed by tunneling spectroscopy in various systems, such as two-dimensional electron gas (2DEG) systems [16,17], carbon nanotubes [18], semiconducting nanowires [19-22], and monolayer graphene [23-26], while only a few studies have observed ABS in long junctions [27,28]. Moreover, there have been no systematic attempts to verify the relationship between the number of ABS pairs and the ratio L/ξ0. To study ABS in different junction limits in more detail, we propose a new system that allows in situ control of ξ0 while simultaneously observing ABS.

In this Letter, we adopted bilayer graphene (BLG) as a normal weak link in an SNS JJ to study the crossover between short and long junction limits by controlling ξ0. The low-energy bands of BLG exhibit approximately quadratic dispersion E≈p2/2me* at small momentum [29], so the Fermi velocity is given by vF=1ℏ∂E∂kF=ℏπnme*, where me* is the effective mass of an electron, and n is the carrier density. We used in situ electrostatic gating to control νF, and hence ξ0. Note that monolayer graphene was not considered for our study due to its linear dispersion, which has a constant νF.

Figure 1 (a) A schematic of Andreev bound states (ABS). (b) Energy-phase relationship of ABS at various ratios between the junction length L and the superconducting coherence length ξ0. (c) A schematic of a loop-type Josephson junction (JJ) device (LD) with the measurement configuration. (d) Backgate voltage (Vbg) dependence of the Fermi velocity (νF) estimated from the Shubnikov–de Haas oscillation from two-terminal type JJ devices (TD; see Fig. S1(a) in Supplemental Material). (e) Backgate voltage dependence of L/ξ0 calculated for different superconducting materials with νF from (d) and L = 1 μm.

In a microscopic mechanism of Josephson coupling, electrons and Andreev-reflected holes go through consecutive Andreev reflections at the superconducting contacts and transport Cooper pairs from one superconductor to the other (Fig. 1(a)). This roundtrip of quasiparticles results in bound states, which are called ABS. The ABS follows the Bohr–Sommerfeld quantization rule [2]:

2cos-1EΔ+Lξ0EΔ±φ=2πN,

where φ=φL-φR is the superconducting phase difference between the left (L) and right (R) superconductors, and N is an integer. This relation can be modified with a scatterer in the normal channel with transparency τ [30,31]. In a short junction limit, the energy–phase relationship of ABS is simply described as E1±=±Δ1-τsin2(φ2) [30,32]. In a long junction limit, however, there is no analytic expression for the ABS energy.

We fabricated two types of JJs: one with a superconducting loop for biasing the superconducting phase difference (LD) and the other for biasing current through the device (TD), both having the same length (L = 1 μm) and width (W = 1.5 μm) (see Fig. S1(a) in the Supplemental Material [33]). First, we encapsulated BLG in between two hexagonal boron nitride (h-BN) sheets to protect the BLG from any chemical impurities during nanofabrication [51]. Then, 70-nm-thick Al superconducting electrodes together with a 6-nm-thick Ti adhesion layer were deposited onto the freshly etched edge of the BLG [34,51]. Lastly, superconducting side tunnel contacts were made with the deposition of 70-nm-thick Al electrodes on the edge of the BLG. When Al contacts graphene directly, a potential barrier should form between the Al and graphene [25,52], so that only quantum tunneling can occur at a low temperature. Tunneling conductance was measured by biasing the current I and measuring the voltage difference V between the tunneling probe and superconducting loop, as depicted in Fig. 1(c). The backgate voltage Vbg was applied to BLG via a 300-nm-thick SiO2 dielectric layer and 26-nm-thick bottom h-BN layer to modulate the carrier density and Fermi velocity of quasiparticles in the BLG. The data were all measured at T = 17 mK, except Fig. S7 in the Supplemental Material [33].

Modulation of the Fermi velocity was confirmed from the temperature dependence of the Shubnikov–de Haas oscillation (SdHO) measured at the device TD The device TD shares the same BLG as the device LD for consistency in quality. The SdHO amplitude was fitted to the Lifshitz–Kosevich formula [38,39] from temperature T = 1.5 to 50 K to estimate the effective mass me* of quasiparticles in BLG. With quadratic energy dispersion of BLG, the Fermi velocity vF=ℏkF/me* was calculated as a function of Vbg and fitted to the theoretical model as shown in Fig. 1(d) (see Figs. S3–4 in the Supplemental Material [33]) [29,53]. The charge neutral point (CNP) at Vbg = –7.2 V was determined from the two-terminal resistance as a function of Vbg of the device TD, which was also adopted for the CNP of the device LD. With the estimated νF, we also calculated L/ξ0 as a function of Vbg assuming various kinds of superconductor with L = 1 μm [Fig. 1(e)]. As BLG is in a ballistic limit away from the CNP, we used the relation ξ0=ℏvF/2Δ (see Fig. S2(b) in the Supplemental Material [33]). Since the maximum Vbg before the dielectric breakdown of the SiO2 layer is around 100 V, Al has the right size of superconducting gap (Δ = 129 μeV) to observe the crossover from the short to long junction limit.

Figure 2 (a) Elastic tunneling of an electron from a superconducting tunneling probe to the Andreev bound state (ABS) in bilayer graphene (BLG) when eV=ΔTP+E+. (b) (Left panel) Phase (φ) dependence of the upper (red line) and lower (blue line) ABS energies in a short junction limit with perfect transparency. (Right panel) Expected tunneling conductance (dI/dV) peak voltage V as a function of φ. (c) Color plots of dI/dV as a function of the bias voltage V and magnetic field B for different backgate voltages Vbg measured in device LD. (d) A color map of dI/dV as a function of the bias voltage (V) and Vbg at fixed φ=0. The red dashed curve represents E1- theoretically calculated from (f). (e–f) Theoretical simulations for (c–d) with L/ξ0 obtained from device TD, respectively.

Tunneling spectroscopy has recently been applied to graphene-based devices with normal [23,24] and superconducting [16,18,25,54] tunneling probes. The superconducting tunneling probe allows higher spectroscopy energy resolution than using a normal probe due to the sharp density of states (DOS) peaks near the superconducting gap edges. With the biased energy eV=ΔTP+E+, as depicted in Fig. 2(a), the filled DOS peak of the probe (denoted by ΔTP) aligns with the empty DOS peak of the upper ABS (denoted by E+), where a tunneling differential conductance (dI/dV) peak is expected. The dI/dV peak does not simply represent the DOS of ABS, but it is determined by the convolution of the DOS of the probe and that of the sample [16,18,25,26]. Figure 2(b) shows the phase dependence of the ABS energy and expected dI/dV peak positions that are offset by ΔTP. Figure 2(c) shows color maps of dI/dV as a function of V and φ at Vbg = 30, –5, and –7.5 V (left to right). The amplitude of the modulation of the dI/dV peaks with φ corresponds to the induced gap ΔLD = 129 μeV, and the offset of the modulation corresponds to the gap energy of the tunnel probe ΔTP = 185 μeV. The superconducting phase difference φ=2πΦ/Φ0=2πB-B0AΦ0 was controlled by external magnetic field B, with loop area A and magnetic flux quantum Φ0. The offset B0 = –0.72 G is determined by considering the center of the Fraunhofer diffraction pattern of the device TD (see Fig. S2 in the Supplemental Material [33]). The ABS oscillation period is 0.86 G, which is consistent with Φ0/A=0.85 G with A ~24 μm2.

By tuning the gate voltages, we observed crossover from the short to long junction limit. At Vbg = 30 V, there is only one ABS pair (N = 1) oscillating within the gap ΔLD, which indicates that the junction is in the short junction limit. This is consistent with the expectation of L/ξ0 ~0.5 being smaller than 1. As the gate voltage approaches VCNP, the second (N = 2) and third (N = 3) ABS pairs gradually appear, and the amplitude of the dI/dV peak oscillation decreases. At Vbg = –5 V, the second ABS (E2-), which oscillates out-of-phase with the first ABS (E1-), is clearly seen. Near the CNP (Vbg = –7.5 V), the third ABS (E3-) starts to appear and the oscillation amplitude becomes very small. We could not observe ABS pairs with N ≥ 4 due to the limited energy resolution. Nonetheless, adopting larger gap superconductors such as TaN (0.7 meV) [55], Nb (1 meV) [35,56,57], or MoRe (1.4 meV) [34,58] might be a viable approach to study higher modes of ABS. We also measured the gate voltage dependence of dI/dV at a fixed phase difference φ=0 to clarify the variance in E1-, as shown in Fig. 2(d). The positions of the dI/dV peak (E1-) gradually decrease as Vbg approaches VCNP. The decrease becomes noticeable at Vbg < 5 V, indicating the increase in L/ξ0 beyond unity.

For more quantitative analysis, we introduced a theoretical model for ABS considering the geometrical asymmetry of the tunnel contact as an effective scatterer (see the section S6 in the Supplemental Material [33]). The numerical simulation on ABS (Figs. 2(e) and (f)) using the vF value obtained in the device TD (red solid line in Fig. 1(e)), and the transparency τ = 0.56~0.9, successfully demonstrate the decrease in ABS energy and reduction in oscillation amplitude near the CNP. Our simulation results also explain the energy gaps between E2- and E3- at φ=πn in Figs. 2(c) and (e), which occur due to the low transparency near the CNP [30,31]. However, the dI/dV peaks at Vbg < 10 V are located at a slightly lower bias voltage and are broader than the theoretical peaks. This can be understood as the mean free path (lm) of the BLG becoming shorter than the channel length when the carrier density approaches the CNP. This demands that the superconducting coherence length in a diffusive limit ξ0=ℏD/Δ be much shorter than ξ0 in a ballistic limit, resulting in the increase in L/ξ0. Here, D=vFlm/2 is the Einstein diffusion coefficient.

Figure 3 (a), (c) Phase (φ) dependence of the ABS energies extracted from the dI/dV peaks at Vbg = 30 and –5 V, respectively (Data). Solid black curves are theoretical fits (Theory). (b), (d) Current–phase relations calculated from the ABS energies in (a) and (c), respectively. (e) Comparison of the Fermi velocities in devices LD and TD as a function of Vbg. (f) Transparency τ of device LD as a function of Vbg.

The current–phase relationship (CPR) can reveal more characteristics of the Josephson supercurrent. In a zero-temperature limit, the Josephson current can be obtained by summing the contributions from the Nth ABS that are filled below the Fermi level, IJ=NIN, where IN=-2eh∂EN-∂φ. From this, we can estimate the Josephson current of the junction by extracting EN- from the data for the short (N = 1) and long (N ≥ 2) junction limits. We obtained ABS energies using the approximation EN-~-(eVABS,N--ΔTP) instead of performing a deconvolution of the measured dI/dV. Here, eVABS,N- represents the bias energy at which the dI/dV peak occurs by the ABS below the Fermi level. From the extracted EN-, one can derive the phase dependence of IJ in the junction [18,23].

Figure 3(a) shows the extracted EN± at Vbg = 30 V and their theoretical fits with Lξ0=0.56 and τ=0.9. In Fig. 3(b), the calculated IJ (denoted as Data) from EN± also shows good agreement with the theory (calculated from the theoretical fit in Fig. 3(a)). The oscillation of IJ mainly follows E1-, since E2- is not dominant here (IJ ~ I1). From Lξ0 and τ, we can deduce that the device LD at Vbg = 30 V is indeed in the short junction and ballistic limit. In comparison, Figs. 3(c) and (d) show the case when E2- is also dominant (Vbg = –5 V). The theoretical calculations fit the data well with Lξ0=2.79 and τ=0.37, indicating that the junction is in the long junction. In Fig. 3(d), I1 is mostly canceled out by I2, which oscillates in antiphase to I1, resulting in the suppressed IJ. This indicates that the total Josephson current decreases as N increases, and it also oscillates when N is even or odd. To quantify the IJ in Figs. 3(b) and (d), the number of conduction channels in BLG M ~ 2W/λF was also considered, where λF is the Fermi wavelength of electrons. M can vary from ~ 60 to 260 with Vbg ranging from –5 to 30V. At Vbg = –5 V, the full participation of E2- strongly suppresses the total Josephson current, even considering the fourfold reduction in the channel number.

Analyzing CPR in monolayer graphene and 2DEG-based JJs has been important for verifying the τ of the junction [16,23]. In our BLG JJ, the Fermi velocity is also important as a fitting parameter, allowing us to reconfirm the variation in ξ0 in the device LD. Fig. 3(e) compares the two Fermi velocities estimated for each TD (the fitted vF in Fig. 1(e)) and LD. Note that the two vF estimated for both devices show a similar trend depending on Vbg. In Fig. 3(f), the transparency τ in the device LD also has strong dependence on the gate voltage, especially near the CNP, suggesting that Andreev pairs are affected by inhomogeneous electron-hole puddles in the BLG channels, as we discussed in Fig. 2.

In conclusion, we achieved in situ control of the ABS number by exploiting the parabolic energy bands of BLG as a weak link in the JJ. Modulating the carrier density from far to near the CNP, L/ξ0 was varied from 0.5 to 5 without changing the channel length or replacing the superconducting material. The gate dependence of the tunneling conductance showed short-to-long junction crossover in a single device, demonstrating that the ABS number varies according to L/ξ0. In the CPR analysis, precise Fermi velocity and transparency values were extracted, and it was shown that the even pairs of ABS strongly suppress the Josephson current. This work provides new possibilities in Andreev-multi-level physics by tuning the Fermi velocity.

Acknowledgments

This work was supported by National Research Foundation (NRF) grants (Nos. 2021R1A6A1A10042944, 2022M3H4A1A04074153, RS-2023-00207732, RS-2023-00208291, No. 2023M3K5A1094810, No. 2023M3K5A1094813) and ITRC program (IITP-2022-RS-2022-00164799) funded by the Ministry of Science and ICT, the Air Force Office of Scientific Research under Award No. FA2386-22-1-4061, Institute of Basic Science under project code IBS-R014-D1, Samsung Science and Technology Foundation under Project Number SSTF-BA2002-05, and Samsung Electronics Co., Ltd. (IO201207-07801-01). G.-H. P. was supported by the Basic Science Research Institute Fund (Grant No. 2021R1A6A1A10042944). K.W. and T.T. acknowledge support from the JSPS KAKENHI (Grant Numbers 21H05233 and 23H02052) and World Premier International Research Center Initiative (WPI), MEXT, Japan.

Authors’ e-mail

*To whom all correspondence should be addressed: lghman@postech.ac.kr (G.-H.L.)

References

[1]	A. F. Andreev, Sov. Phys. JETP 19, 1228 (1964).

[2]	I. O. Kulik, Sov. Phys. JETP 30, 944 (1970).

[3]	K. K. Likharev, Rev. Mod. Phys. 51, 101 (1979).

[4]	F. Pientka, A. Keselman, E. Berg, A. Yacoby, A. Stern, and B. I. Halperin, Phys. Rev. X 7, 021032 (2017).

[5]	M. Hell, M. Leijnse, and K. Flensberg, Phys. Rev. Lett. 118, 107701 (2017).

[6]	T. H. Hsieh and L. Fu, Phys. Rev. Lett. 108, 107005 (2012).

[7]	A. Zazunov, V. S. Shumeiko, E. N. Bratus’, J. Lantz, and G. Wendin, Phys. Rev. Lett. 90, 087003 (2003).

[8]	C. Janvier et al., Science 349, 1199 (2015).

[9]	L. Bretheau, Ç. Ö. Girit, H. Pothier, D. Esteve, and C. Urbina, Nature 499, 312 (2013).

[10]	J. J. A. Baselmans, A. F. Morpurgo, B. J. van Wees, and T. M. Klapwijk, Nature 397, 43 (1999).

[11]	N. M. Chtchelkatchev and Y. V. Nazarov, Phys. Rev. Lett. 90, 226806 (2003).

[12]	E. Strambini, S. D'Ambrosio, F. Vischi, F. S. Bergeret, Y. V. Nazarov, and F. Giazotto, Nat. Nanotechnol. 11, 1055 (2016).

[13]	P. M. Tam and C. L. Kane, Phys. Rev. Lett. 130, 096301 (2023).

[14]	P. M. Tam, C. De Beule, and C. L. Kane, Phys. Rev. B 107, 245422 (2023).

[15]	I. V. Borzenets et al., Phys. Rev. Lett. 117, 237002 (2016).

[16]	F. Nichele et al., Phys. Rev. Lett. 124, 226801 (2020).

[17]	C. M. Moehle et al., Nano Lett. 22, 8601 (2022).

[18]	J. D. Pillet, C. H. L. Quay, P. Morfin, C. Bena, A. L. Yeyati, and P. Joyez, Nat. Phys. 6, 965 (2010).

[19]	W. Chang, V. E. Manucharyan, T. S. Jespersen, J. Nygård, and C. M. Marcus, Phys. Rev. Lett. 110, 217005 (2013).

[20]	D. J. van Woerkom et al., Nat. Phys. 13, 876 (2017).

[21]	A. Pöschl, A. Danilenko, D. Sabonis, K. Kristjuhan, T. Lindemann, C. Thomas, M. J. Manfra, and C. M. Marcus, Phys. Rev. B 106, L241301 (2022).

[22]	A. Pöschl, A. Danilenko, D. Sabonis, K. Kristjuhan, T. Lindemann, C. Thomas, M. J. Manfra, and C. M. Marcus, Phys. Rev. B 106, L161301 (2022).

[23]	L. Bretheau, J. I. J. Wang, R. Pisoni, K. Watanabe, T. Taniguchi, and P. Jarillo-Herrero, Nat. Phys. 13, 756 (2017).

[24]	J. I.-J. Wang, L. Bretheau, D. Rodan-Legrain, R. Pisoni, K. Watanabe, T. Taniguchi, and P. Jarillo-Herrero, Phys. Rev. B 98, 121411(R) (2018).

[25]	S. Park et al., Nature 603, 421 (2022).

[26]	T. Dirks, T. L. Hughes, S. Lal, B. Uchoa, Y.-F. Chen, C. Chialvo, P. M. Goldbart, and N. Mason, Nat. Phys. 7, 386 (2011).

[27]	L. Tosi, C. Metzger, M. F. Goffman, C. Urbina, H. Pothier, S. Park, A. L. Yeyati, J. Nygård, and P. Krogstrup, Phys. Rev. X 9, 011010 (2019).

[28]	P. Zellekens, R. S. Deacon, P. Perla, D. Grützmacher, M. I. Lepsa, T. Schäpers, and K. Ishibashi, Commun. Phys. 5, 267 (2022).

[29]	M. Edward and K. Mikito, Rep. Prog. Phys. 76, 056503 (2013).

[30]	P. F. Bagwell, Phys. Rev. B 46, 12573 (1992).

[31]	P. Samuelsson, J. Lantz, V. S. Shumeiko, and G. Wendin, Phys. Rev. B 62, 1319 (2000).

[32]	C. W. J. Beenakker, Phys. Rev. Lett. 67, 3836 (1991).

[33]	See Supplemental Material at [URL], which includes Refs. [34–50].

[34]	V. E. Calado, S. Goswami, G. Nanda, M. Diez, A. R. Akhmerov, K. Watanabe, T. Taniguchi, T. M. Klapwijk, and L. M. K. Vandersypen, Nat. Nanotechnol. 10, 761 (2015).

[35]	M. Ben Shalom et al., Nat. Phys. 12, 318 (2016).

[36]	J. Park, J. H. Lee, G.-H. Lee, Y. Takane, K.-I. Imura, T. Taniguchi, K. Watanabe, and H.-J. Lee, Phys. Rev. Lett. 120, 077701 (2018).

[37]	C. Handschin, P. Makk, P. Rickhaus, M.-H. Liu, K. Watanabe, T. Taniguchi, K. Richter, and C. Schönenberger, Nano Lett. 17, 328 (2017).

[38]	K. Zou, X. Hong, and J. Zhu, Phys. Rev. B 84, 085408 (2011).

[39]	J. Li, L. Z. Tan, K. Zou, A. A. Stabile, D. J. Seiwell, K. Watanabe, T. Taniguchi, S. G. Louie, and J. Zhu, Phys. Rev. B 94, 161406(R) (2016).

[40]	J. W. McClure, Phys. Rev. 108, 612 (1957).

[41]	J. C. Slonczewski and P. R. Weiss, Phys. Rev. 109, 272 (1958).

[42]	J. W. McClure, Phys. Rev. 119, 606 (1960).

[43]	C. W. J. Beenakker, Phys. Rev. Lett. 97, 067007 (2006).

[44]	G. B. Lesovik and I. A. Sadovskyy, Phys.-Usp. 54, 1007 (2011).

[45]	M. Barbier, P. Vasilopoulos, and F. M. Peeters, Phys. Rev. B 82, 235408 (2010).

[46]	S. Pinon, V. Kaladzhyan, and C. Bena, Phys. Rev. B 101, 205136 (2020).

[47]	J. A. Sauls, Phil. Trans. R. Soc. A 376, 20180140 (2018).

[48]	M. Titov and C. W. J. Beenakker, Phys. Rev. B 74, 041401 (2006).

[49]	T. Ludwig, Phys. Rev. B 75, 195322 (2007).

[50]	I. Snyman and C. W. J. Beenakker, Phys. Rev. B 75, 045322 (2007).

[51]	L. Wang et al., Science 342, 614 (2013).

[52]	G.-H. Lee, S. Kim, S.-H. Jhi, and H.-J. Lee, Nat. Commun. 6, 6181 (2015).

[53]	E. McCann and V. I. Fal’ko, Phys. Rev. Lett. 96, 086805 (2006).

[54]	M. Meschke, J. T. Peltonen, J. P. Pekola, and F. Giazotto, Phys. Rev. B 84, 214514 (2011).

[55]	M. Müller, R. Hoepfl, L. Liensberger, S. Geprägs, H. Huebl, M. Weiler, R. Gross, and M. Althammer, Mater. Quantum. Technol. 1, 045001 (2021).

[56]	P. Rickhaus, M. Weiss, L. Marot, and C. Schönenberger, Nano Lett. 12, 1942 (2012).

[57]	G.-H. Park, M. Kim, K. Watanabe, T. Taniguchi, and H.-J. Lee, Sci. Rep. 7, 10953 (2017).

[58]	F. Amet et al., Science 352, 966 (2016).